SIKA SPECIFICATION NOTE: This guide specification is provided in CSI Format for use by design professionals for individual construction projects. Modify the text based on your project requirements, and delete products not required. Questions? Call 800-933-SIKA.

SIKA SPECIFICATION NOTE: This guide specification includes test methods, materials and installation procedures for Sikalastic Polyurethane Traffic Coatings, a cold applied, highly durable, seamless, fully bonded, elastomeric polyurethane waterproofing and traffic bearing membrane which is applied direct to concrete, plywood, and existing traffic coatings, and is intended for direct pedestrian traffic.

SECTION 07 18 13

PEDESTRIAN TRAFFIC COATINGS

1. GENERAL
	* + 1. RELATED DOCUMENTS
				1. Drawings and general provisions of the Contract, including General and Supplementary Conditions and Division 01 Specification Sections, apply to this Section.
			2. SUMMARY
				1. Provide a polyurethane traffic coating system as specified and as indicated on the Drawings.
				2. Related Work: The following items are not included in this Section and are specified under the designated Sections:

Section 03 30 00 – CAST-IN-PLACE CONCRETE.

Section 06 16 00 – SHEATHING.

Section 07 60 00 – FLASHING AND SHEET METAL.

Section 07 92 13 – ELASTOMERIC JOINT SEALANTS.

Section 22 14 26 – PLAZA DRAINS.

* + - 1. PERFORMANCE REQUIREMENTS
				1. Cold fluid applied polyurethane roofing traffic waterproofing system is intended to perform as a continuous barrier against liquid water and to flash or discharge to the incidental water. Membrane system shall accommodate movements of building materials as required with accessory sealant materials at such locations, changes in substrate, perimeter conditions and penetrations.
				2. Installed waterproofing membrane/surfacing system shall not permit the passage of water, and will withstand the anticipated traffic wear exposures in accordance with the most current revision of ASTM C957, High-Solids Content, Cold Liquid-Applied Elastomeric Waterproofing Membrane with Integral Wearing Surface.
				3. Intent is to bridge and seal the following air and water leakage pathways and gaps:

Connections of the walls to the deck.

Piping, conduit, duct and similar penetrations.

All other air leakage and water intrusion pathways to building envelope connections.

* + - 1. SUBMITTALS
				1. Submittals: Comply with project requirements for submittals as specified in Division 01.
				2. Product Data:

Materials list of items proposed to be provided under this Section.

Manufacturer's specifications and other data needed to prove compliance with the specified requirements.

Drawings or catalog illustrations in sufficient detail to show installation and interface of the work of this Section with the work of adjacent trades.

Manufacturer's current recommended installation procedures.

* + - * 1. Mock-Ups: Provide a mock-up on site to demonstrate workmanship and final appearance. Locate in an area acceptable to the Architect. Accepted mock-up may remain in place.
			1. QUALITY ASSURANCE
				1. Installer Qualifications:

Installer shall have at least three years of experience in installing materials of types specified and shall have successfully completed at least three projects of similar scope and complexity.

Installer shall designate a single individual as project foreman who shall be on site at all times during installation.

* + - * 1. Field Adhesion Test Method: Use manufacturer's standard field adhesion test methods and methods to verify proper priming and surface preparation techniques required to obtain optimum adhesion. Evaluate and report results of field adhesion testing.
				2. Waterproofing Terminology: Refer to ASTM D1079 and Sikalastic Deck Pro Applicator Manual for definitions of waterproofing terms related to this section.
			1. PRE-INSTALLATION CONFERENCE
				1. Prior to scheduled commencement of installation and associated work, conduct a meeting at the project site with the installer, architect/consultant, owner, manufacturer’s representative and any other persons directly involved with the performance of the Work. The Installer shall record conference discussions and to include decisions and agreements reached (or disagreements), and furnish copies of recorded discussions to each attending party. The main purpose of this meeting is to review foreseeable methods and procedures related to the Work.
			2. REGULATORY REQUIREMENTS
				1. Applicable Regulations: Comply with local code and requirements of authorities having jurisdiction. Do not exceed VOC regulations as established by the State in which they are being installed; including total VOC content, in grams per liter, for all system components (i.e. primers, adhesives, coatings, and similar items.)
			3. DELIVERY, STORAGE AND HANDLING
				1. Deliver materials to the job site in the manufacturer's unopened containers with all labels intact and legible at time of use. Handle and store materials in accordance with manufacturer's recommendations with proper precautions to ensure fitness of material when installed.
			4. WARRANTY
				1. Warranty: Provide manufacturer’s standard warranty for each type of product. Include written testing documentation and test reports if requested by Architect.
1. PRODUCTS
	* + 1. MANUFACTURER
				1. Basis-of-Design Manufacturer: Sika Corporation, 201 Polito Avenue, Lyndhurst NJ 07071. Toll Free 800-933-SIKA (7452), www.usa.sika.com. No substitutions without prior written approval by the Architect.
			2. TRAFFIC COATINGS (SIKALASTIC 710/715 TRAFFIC SYSTEM)
				1. Pedestrian Traffic Coating: Sikalastic 710/715 Traffic System comprised of the following:

Primers :

Sikalastic Primer 1C fast curing PU primer.

Sikalastic FTP water-based epoxy primer.

Sikalastic FTP LoVOC 100% solids epoxy primer (as a standard primer and for recoat applications and elevated moisture content up to 6% by Tramex ).

Sikalastic PF Lo-VOC 100% solids epoxy primer (for rough and/or porous substrates).

Sikalastic MT 100% solids epoxy primer (for substrates with elevated moisture content up to 6 % by Tramex ).Sikalastic 710 Base one-component aromatic polyurethane base coat.

Sikalastic 715 Top one-component aromatic polyurethane top coat.

Sikalastic 700 ACL accelerator (optional).

Sikalastic 735 AL, and 748 PA aliphatic top coats (optional).

* + - * 1. Applied Total Dry Film Thickness Exclusive of Aggregate:

Pedestrian Traffic: 33 mils.

Heavy Pedestrian Traffic: 43 mils.

* + - * 1. Aggregate:

Standard Aggregate: Clean, rounded, oven dried quartz sand with a minimum gradation of 16-30 mesh or 20-40 mesh for pedestrian traffic, and a minimum hardness of 6.5 per the Moh’s scale. Aggregate shall be supplied in pre-packaged bags and free of metallic or other impurities.

Decorative Aggregate: UV-stable, ceramic-coated quartz aggregate in a standard or custom color blend. Intended for a full broadcast application where a clear sealcoat will be applied. Aggregate shall be supplied in pre-blended and packaged bags.

* + - * 1. Flakes:

Decorative Flakes: UV-stable, vinyl flakes in a standard or custom color blend. Intended for a partial or full broadcast application where a clear sealcoat will be applied. Flakes shall be supplied in pre-blended and packaged bags.

* + - * 1. Fabric Reinforcement: Sikalastic Flexitape Heavy woven nylon reinforcement.
				2. Base and Top Coats: Typical Physical properties complying with the following.

Sikalastic 710 Base 715 Top

Viscosity 6500 +/- 3000 cps 1500 +/- 500 cps

Total Volume Solids (ASTM D2697) 71% 72%

VOC Content (ASTM D2369) 240 g/l 243 g/l

Tensile Strength (ASTM D412) 500 +/- 100 psi 3200 +/- 300 psi

Elongation at Break (ASTM D412) 800 +/- 50% 500 +/- 50%

Tear Resistance (Die C, ASTM D624) 250 +/- 25 pli 350 +/- 50 pli

Hardness (ASTM D2240) 55 +/- 5 Shore A 85 +/- 5 Shore A

Tests were performed with material and curing conditions at 75F and 50% relative humidity.

* + - * 1. Aliphatic Top Coats (Optional): Physical properties complying with the following.

Sikalastic 735 AL 748 PA

Viscosity 2500 +/- 700 cps 200 +/- 50 cps

Total Volume Solids (ASTM D2697) 74% 78%

VOC Content (ASTM D2369) 225 g/l 100 g/l

Tensile Strength (ASTM D412) 4200 +/- 300 psi 2500 +/- 200 psi

Elongation at Break (ASTM D412) 230 +/- 50% 100 +/- 25%

Tear Resistance (Die C, ASTM D624) 400 +/- 50 pli 300 +/- 50 pli

Hardness (ASTM D2240) 90 +/- 5 Shore A 50 +/- 5 Shore D

Tests were performed with material and curing conditions at 75F and 50% relative humidity.

* + - 1. TRAFFIC COATINGS (SIKALASTIC 710 NP/715 TRAFFIC SYSTEM)
				1. Pedestrian Traffic Coating: Sikalastic 710 NP/715 Traffic System ( primerless ) comprised of the following:

Sikalastic 710 NP Base one-component aromatic polyurethane primerless base coat.

Sikalastic 715 Top one-component aromatic polyurethane top coat.

Sikalastic 700 ACL accelerator (optional).

Sikalastic 735 AL, and 748 PA aliphatic top coats (optional).

* + - * 1. Applied Total Dry Film Thickness Exclusive of Aggregate:

Pedestrian Traffic: 33 mils.

Heavy Pedestrian Traffic: 43 mils.

* + - * 1. Aggregate:

Standard Aggregate: Clean, rounded, oven dried quartz sand with a minimum gradation of 16-30 mesh or 20-40 mesh for pedestrian traffic, and a minimum hardness of 6.5 per the Moh’s scale. Aggregate shall be supplied in pre-packaged bags and free of metallic or other impurities.

Decorative Aggregate: UV-stable, ceramic-coated quartz aggregate in a standard or custom color blend. Intended for a full broadcast application where a clear sealcoat will be applied. Aggregate shall be supplied in pre-blended and packaged bags.

* + - * 1. Flakes:

Decorative Flakes: UV-stable, vinyl flakes in a standard or custom color blend. Intended for a partial or full broadcast application where a clear sealcoat will be applied. Flakes shall be supplied in pre-blended and packaged bags.

* + - * 1. Fabric Reinforcement: Sikalastic Flexitape Heavy woven nylon reinforcement.
				2. Base and Top Coats: Typical Physical properties complying with the following.

Sikalastic 710 NP Base 715 Top

Viscosity 6500 +/- 3000 cps 1500 +/- 500 cps

Total Volume Solids (ASTM D2697) 71% 72%

VOC Content (ASTM D2369) 240 g/l 243 g/l

Tensile Strength (ASTM D412) 650 +/- 100 psi 3200 +/- 300 psi

Elongation at Break (ASTM D412) 375 +/- 50% 500 +/- 50%

Tear Resistance (Die C, ASTM D624) 170 +/- 25 pli 350 +/- 50 pli

Hardness (ASTM D2240) 55 +/- 5 Shore A 85 +/- 5 Shore A

Tests were performed with material and curing conditions at 75F and 50% relative humidity.

* + - * 1. Aliphatic Top Coats (Optional): Typical Physical properties complying with the following.

Sikalastic 735 AL 748 PA

Viscosity 2500 +/- 700 cps 200 +/- 50 cps

Total Volume Solids (ASTM D2697) 74% 78%

VOC Content (ASTM D2369) 225 g/l 100 g/l

Tensile Strength (ASTM D412) 4200 +/- 300 psi 2500 +/- 200 psi

Elongation at Break (ASTM D412) 230 +/- 50% 100 +/- 25%

Tear Resistance (Die C, ASTM D624) 400 +/- 50 pli 300 +/- 50 pli

Hardness (ASTM D2240) 90 +/- 5 Shore A 50 +/- 5 Shore D

Tests were performed with material and curing conditions at 75F and 50% relative humidity.

* + - 1. TRAFFIC COATINGS (SIKALASTIC 710/715 Textured TRAFFIC SYSTEM)
				1. Pedestrian Traffic Coating: Sikalastic 710/715 Textured Traffic System comprised of the following:

Primers :

Sikalastic Primer 1C fast curing PU primer.

Sikalastic FTP water-based epoxy primer.

Sikalastic FTP LoVOC 100% solids epoxy primer (as a standard primer and for recoat applications and elevated moisture content up to 6% by Tramex ).

Sikalastic PF Lo-VOC 100% solids epoxy primer (for rough and/or porous substrates).

Sikalastic MT 100% solids epoxy primer (for substrates with elevated moisture content up to 6 % by Tramex ).Sikalastic 710 Base one-component aromatic polyurethane base coat.

Sikalastic 710 Base one-component aromatic polyurethane base coat.

Sikalastic 715 Textured one-component aromatic polyurethane top coat with integrated aggregate.

Sikalastic 700 ACL accelerator (optional).

* + - * 1. Applied Total Dry Film Thickness Exclusive of Aggregate:

Pedestrian Traffic: 33 mils.

Heavy Pedestrian Traffic: 43 mils.

* + - * 1. Fabric Reinforcement: Sikalastic Flexitape Heavy woven nylon reinforcement.
				2. Base and Top Coats: Typical Physical properties complying with the following.

Sikalastic 710 Base 715 Textured

Viscosity 6500 +/- 3000 cps 1500 +/- 500 cps

Total Volume Solids (ASTM D2697) 71% 72%

VOC Content (ASTM D2369) 240 g/l 243 g/l

Tensile Strength (ASTM D412) 500 +/- 100 psi 3200 +/- 300 psi

Elongation at Break (ASTM D412) 800 +/- 50% 500 +/- 50%

Tear Resistance (Die C, ASTM D624) 250 +/- 25 pli 350 +/- 50 pli

Hardness (ASTM D2240) 55 +/- 5 Shore A 85 +/- 5 Shore A

Tests were performed with material and curing conditions at 75F and 50% relative humidity.

* + - 1. TRAFFIC COATINGS (SIKALASTIC 710 NP/715 Textured)
				1. Pedestrian Traffic Coating: Sikalastic 710 NP/715 Textured Traffic System ( primerless ) comprised of the following:

Sikalastic 710 NP Base one-component aromatic polyurethane primerless base coat.

Sikalastic 715 Textured one-component aromatic polyurethane top coat with integrated aggregate.

Sikalastic 700 ACL accelerator (optional).

* + - * 1. Applied Total Dry Film Thickness Exclusive of Aggregate:

Pedestrian Traffic: 33 mils.

Heavy Pedestrian Traffic: 43 mils.

* + - * 1. Fabric Reinforcement: Sikalastic Flexitape Heavy woven nylon reinforcement.
				2. Base and Top Coats: Typical Physical properties complying with the following.

Sikalastic 710 NP Base 715 Textured

Viscosity 6500 +/- 3000 cps 1500 +/- 500 cps

Total Volume Solids (ASTM D2697) 71% 72%

VOC Content (ASTM D2369) 240 g/l 243 g/l

Tensile Strength (ASTM D412) 650 +/- 100 psi 3200 +/- 300 psi

Elongation at Break (ASTM D412) 375 +/- 50% 500 +/- 50%

Tear Resistance (Die C, ASTM D624) 170 +/- 25 pli 350 +/- 50 pli

Hardness (ASTM D2240) 55 +/- 5 Shore A 85 +/- 5 Shore A

Tests were performed with material and curing conditions at 75F and 50% relative humidity.

Tests were performed with material and curing conditions at 75F and 50% relative humidity.

* + - 1. TRAFFIC COATINGS (SIKALASTIC 710/22 Lo-Mod HYBRID TRAFFIC SYSTEM)
				1. Pedestrian Traffic Coating: Sikalastic 710/22 Lo-Mod Hybrid Traffic System comprised of the following:

Primers :

Sikalastic Primer 1C fast curing PU primer.

Sikalastic FTP water-based epoxy primer.

Sikalastic FTP LoVOC 100% solids epoxy primer (as a standard primer and for recoat applications and elevated moisture content up to 6% by Tramex ).

Sikalastic PF Lo-VOC 100% solids epoxy primer (for rough and/or porous substrates).

Sikalastic MT 100% solids epoxy primer (for substrates with elevated moisture content up to 6 % by Tramex ).Sikalastic 710 Base one-component aromatic polyurethane base coat.

Sikalastic 710 Base one-component aromatic polyurethane base coat.

Sikadur 22 Lo-Mod low-modulus, medium viscosity epoxy resin binder.

Sikalastic 700 ACL accelerator (optional).

Sikalastic 715 aromatic or 735 AL aliphatic top coats (optional).

* + - * 1. Full Broadcast Method – Applied Total Dry Film Thickness Exclusive of Aggregate and Optional Top Coat:

Heavy Pedestrian Traffic: 43 mils.

* + - * 1. Aggregate: Clean, rounded, oven dried quartz sand with a minimum gradation of 16-30 mesh for vehicular traffic, and a minimum hardness of 6.5 per the Moh’s scale. Aggregate shall be supplied in pre-packaged bags and free of metallic or other impurities.
				2. Fabric Reinforcement: Sikalastic Flexitape Heavy woven nylon reinforcement.
				3. Base Coat: Typical Physical properties complying with the following.

Sikalastic 710 Base

Viscosity 6500 +/- 3000 cps

Total Volume Solids (ASTM D2697) 71%

VOC Content (ASTM D2369) 240 g/l

Tensile Strength (ASTM D412) 500 +/- 100 psi

Elongation at Break (ASTM D412) 800 +/- 50%

Tear Resistance (Die C, ASTM D624) 250 +/- 25 pli

Hardness (ASTM D2240) 55 +/- 5 Shore A

Tests were performed with material and curing conditions at 75°F and 50% relative humidity.

* + - * 1. Wear Coat: Typical Physical properties complying with the following.

Sikadur 22 Lo-Mod

Viscosity 2000 cps / 30 min

Total Volume Solids (ASTM D2697) 100%

VOC Content (ASTM D2369) 56 g/l

Tensile Strength (ASTM D638) 5,700 psi

Elongation at Break (ASTM D638) >30%

Hardness (ASTM D2240) 70 Shore D

Tests were performed with material and curing conditions at 75°F and 50% relative humidity.

* + - * 1. Aromatic Top Coat: Typical Physical properties complying with the following.

Sikalastic 715 Top

Viscosity 1500 +/- 500 cps

Total Volume Solids (ASTM D2697) 72%

VOC Content (ASTM D2369) 243 g/l

Tensile Strength (ASTM D412) 3200 +/- 300 psi

Elongation at Break (ASTM D412) 500 +/- 50%

Tear Resistance (Die C, ASTM D624) 350 +/- 50 pli

Hardness (ASTM D2240) 85 +/- 5 Shore A

Tests were performed with material and curing conditions at 75°F and 50% relative humidity.

* + - * 1. Aliphatic Top Coat: Typical Physical properties complying with the following.

Sikalastic 735 AL

Viscosity 2500 +/- 700 cps

Total Volume Solids (ASTM D2697) 74%

VOC Content (ASTM D2369) 225 g/l

Tensile Strength (ASTM D412) 4200 +/- 300 psi

Elongation at Break (ASTM D412) 230 +/- 50%

Tear Resistance (Die C, ASTM D624) 400 +/- 50 pli

Hardness (ASTM D2240) 90 +/- 5 Shore A

Tests were performed with material and curing conditions at 75°F and 50% relative humidity.

* + - 1. TRAFFIC COATINGS (SIKALASTIC 710NP/22 Lo-Mod HYBRID TRAFFIC SYSTEM)
				1. Pedestrian Traffic Coating: Sikalastic 710NP/22 Lo-Mod Hybrid Traffic System comprised of the following:

Sikalastic 710 NP Base one-component aromatic polyurethane base coat.

Sikadur 22 Lo-Mod low-modulus, medium viscosity epoxy resin binder.

Sikalastic 700 ACL accelerator (optional).

Sikalastic 715 aromatic or 735 AL aliphatic top coats (optional).

* + - * 1. Full Broadcast Method – Applied Total Dry Film Thickness Exclusive of Aggregate and Optional Top Coat:

Heavy Pedestrian Traffic: 43 mils.

* + - * 1. Aggregate: Clean, rounded, oven dried quartz sand with a minimum gradation of 16-30 mesh for vehicular traffic, and a minimum hardness of 6.5 per the Moh’s scale. Aggregate shall be supplied in pre-packaged bags and free of metallic or other impurities.
				2. Fabric Reinforcement: Sikalastic Flexitape Heavy woven nylon reinforcement.
				3. Base Coat: Typical Physical properties complying with the following.

Sikalastic 710 NP Base

Viscosity 6500 +/- 3000 cps

Total Volume Solids (ASTM D2697) 71%

VOC Content (ASTM D2369) 240 g/l

Tensile Strength (ASTM D412) 650 +/- 100 psi

Elongation at Break (ASTM D412) 375 +/- 50%

Tear Resistance (Die C, ASTM D624) 170 +/- 25 pli

Hardness (ASTM D2240) 55 +/- 5 Shore A

Tests were performed with material and curing conditions at 75°F and 50% relative humidity.

* + - * 1. Wear Coat: Physical properties complying with the following.

Sikadur 22 Lo-Mod

Viscosity 2000 cps / 30 min

Total Volume Solids (ASTM D2697) 100%

VOC Content (ASTM D2369) 56 g/l

Tensile Strength (ASTM D638) 5,700 psi

Elongation at Break (ASTM D638) >30%

Hardness (ASTM D2240) 70 Shore D

Tests were performed with material and curing conditions at 75°F and 50% relative humidity.

* + - * 1. Aromatic Top Coat: Typical Physical properties complying with the following.

Sikalastic 715 Top

Viscosity 1500 +/- 500 cps

Total Volume Solids (ASTM D2697) 72%

VOC Content (ASTM D2369) 243 g/l

Tensile Strength (ASTM D412) 3200 +/- 300 psi

Elongation at Break (ASTM D412) 500 +/- 50%

Tear Resistance (Die C, ASTM D624) 350 +/- 50 pli

Hardness (ASTM D2240) 85 +/- 5 Shore A

Tests were performed with material and curing conditions at 75°F and 50% relative humidity.

* + - * 1. Aliphatic Top Coat: Typical Physical properties complying with the following.

Sikalastic 735 AL

Viscosity 2500 +/- 700 cps

Total Volume Solids (ASTM D2697) 74%

VOC Content (ASTM D2369) 225 g/l

Tensile Strength (ASTM D412) 4200 +/- 300 psi

Elongation at Break (ASTM D412) 230 +/- 50%

Tear Resistance (Die C, ASTM D624) 400 +/- 50 pli

Hardness (ASTM D2240) 90 +/- 5 Shore A

Tests were performed with material and curing conditions at 75°F and 50% relative humidity.

* + - 1. TRAFFIC COATINGS (SIKALASTIC 710 Lo-VOC/715 Lo-VOC TRAFFIC SYSTEM)
				1. Pedestrian Traffic Coating: Sikalastic 710 Lo-VOC/715 Lo-VOC Traffic System comprised of the following:

Primers :

Sikalastic Primer 1C fast curing PU primer.

Sikalastic FTP water-based epoxy primer.

Sikalastic FTP LoVOC 100% solids epoxy primer (as a standard primer and for recoat applications and elevated moisture content up to 6% by Tramex ).

Sikalastic PF Lo-VOC 100% solids epoxy primer (for rough and/or porous substrates).

Sikalastic MT 100% solids epoxy primer (for substrates with elevated moisture content up to 6 % by Tramex ).Sikalastic 710 Base one-component aromatic polyurethane base coat.

Sikalastic 710 Lo-VOC Base one-component aromatic polyurethane base coat.

Sikalastic 710 Lo-VOC Booster (optional)

Sikalastic 715 Lo-VOC Top one-component aromatic polyurethane top coat.

Sikalastic 715 Lo-VOC Booster (optional)

Sikalastic 700 ACL accelerator (optional).

Sikalastic 736 AL, and 748 PA aliphatic top coats (optional).

* + - * 1. Applied Total Dry Film Thickness Exclusive of Aggregate:

Pedestrian Traffic: 33 mils.

Heavy Pedestrian Traffic: 43 mils.

* + - * 1. Aggregate:

Standard Aggregate: Clean, rounded, oven dried quartz sand with a minimum gradation of 16-30 mesh or 20-40 mesh for pedestrian traffic, and a minimum hardness of 6.5 per the Moh’s scale. Aggregate shall be supplied in pre-packaged bags and free of metallic or other impurities.

Decorative Aggregate: UV-stable, ceramic-coated quartz aggregate in a standard or custom color blend. Intended for a full broadcast application where a clear sealcoat will be applied. Aggregate shall be supplied in pre-blended and packaged bags.

* + - * 1. Flakes:

Decorative Flakes: UV-stable, vinyl flakes in a standard or custom color blend. Intended for a partial or full broadcast application where a clear sealcoat will be applied. Flakes shall be supplied in pre-blended and packaged bags.

* + - * 1. Fabric Reinforcement: Sikalastic Flexitape Heavy woven nylon reinforcement.
				2. Base and Top Coats: Typical Physical properties complying with the following.

Sikalastic 710 Lo-VOC Base 715 Lo-VOC

Viscosity 6500 +/- 3000 cps 4000 +/- 2000 cps

Total Volume Solids (ASTM D2697) 89% 89%

VOC Content (ASTM D2369) 93 g/l 96 g/l

Tensile Strength (ASTM D412) 1200 +/- 300 psi 3400 +/- 300 psi

Elongation at Break (ASTM D412) 450 +/- 50% 450 +/- 50%

Tear Resistance (Die C, ASTM D624) 195 +/- 25 pli 350 +/- 50 pli

Hardness (ASTM D2240) 75 +/- 5 Shore A 85 +/- 5 Shore A

Tests were performed with material and curing conditions at 75F and 50% relative humidity.

* + - * 1. Aliphatic Top Coats (Optional): Typical Physical properties complying with the following.

Sikalastic 736 AL Lo-VOC 748 PA

Viscosity 3500 +/- 700 cps 200 +/- 50 cps

Total Volume Solids (ASTM D2697) 83% 78%

VOC Content (ASTM D2369) 99 g/l 100 g/l

Tensile Strength (ASTM D412) 4000 +/- 300 psi 2500 +/- 200 psi

Elongation at Break (ASTM D412) 250 +/- 50% 100 +/- 25%

Tear Resistance (Die C, ASTM D624) 400 +/- 50 pli 300 +/- 50 pli

Hardness (ASTM D2240) 90 +/- 5 Shore A 50 +/- 5 Shore D

Tests were performed with material and curing conditions at 75F and 50% relative humidity.

* + - 1. TRAFFIC COATINGS (SIKALASTIC 715 Lo-VOC + SIKALASTIC 715 Lo-VOC Booster / 715 Lo-VOC + SIKALASTIC 715 Lo-VOC Booster Traffic System )
				1. Pedestrian Traffic Coating: Sikalastic 715 Lo-VOC + Sikalastic 715 LoVOC Booster / Sikalastic 715 Lo-VOC + Sikalastic 715 LoVOC Booster Traffic System comprised of the following:

Primers :

Sikalastic Primer 1C fast curing PU primer.

Sikalastic FTP water-based epoxy primer.

Sikalastic FTP LoVOC 100% solids epoxy primer (as a standard primer and for recoat applications and elevated moisture content up to 6% by Tramex ).

Sikalastic PF Lo-VOC 100% solids epoxy primer (for rough and/or porous substrates).

Sikalastic MT 100% solids epoxy primer (for substrates with elevated moisture content up to 6 % by Tramex ).Sikalastic 710 Base one-component aromatic polyurethane base coat.

Sikalastic 715 Lo-VOC Top one-component aromatic polyurethane coat.

Sikalastic 715 Lo-VOC Booster (optional)

Sikalastic 700 ACL accelerator (optional).

Sikalastic 736 AL, and 748 PA aliphatic top coats (optional).

* + - * 1. Applied Total Dry Film Thickness Exclusive of Aggregate:

Pedestrian Traffic: 33 mils.

Heavy Pedestrian Traffic: 43 mils.

* + - * 1. Aggregate:

Standard Aggregate: Clean, rounded, oven dried quartz sand with a minimum gradation of 16-30 mesh or 20-40 mesh for pedestrian traffic, and a minimum hardness of 6.5 per the Moh’s scale. Aggregate shall be supplied in pre-packaged bags and free of metallic or other impurities.

Decorative Aggregate: UV-stable, ceramic-coated quartz aggregate in a standard or custom color blend. Intended for a full broadcast application where a clear sealcoat will be applied. Aggregate shall be supplied in pre-blended and packaged bags.

* + - * 1. Flakes:

Decorative Flakes: UV-stable, vinyl flakes in a standard or custom color blend. Intended for a partial or full broadcast application where a clear sealcoat will be applied. Flakes shall be supplied in pre-blended and packaged bags.

* + - * 1. Fabric Reinforcement: Sikalastic Flexitape Heavy woven nylon reinforcement.
				2. Base and Top Coats: Physical properties complying with the following.

Sikalastic 715 Lo-VOC

Viscosity 4000 +/- 2000 cps

Total Volume Solids (ASTM D2697) 89%

VOC Content (ASTM D2369) 96 g/l

Tensile Strength (ASTM D412) 3400 +/- 300 psi

Elongation at Break (ASTM D412) 450 +/- 50%

Tear Resistance (Die C, ASTM D624) 350 +/- 50 pli

Hardness (ASTM D2240) 85 +/- 5 Shore A

Tests were performed with material and curing conditions at 75F and 50% relative humidity.

* + - * 1. Aliphatic Top Coats (Optional): Physical properties complying with the following.

Sikalastic 736 AL Lo-VOC 748 PA

Viscosity 3500 +/- 700 cps 200 +/- 50 cps

Total Volume Solids (ASTM D2697) 83% 78%

VOC Content (ASTM D2369) 99 g/l 100 g/l

Tensile Strength (ASTM D412) 4000 +/- 300 psi 2500 +/- 200 psi

Elongation at Break (ASTM D412) 250 +/- 50% 100 +/- 25%

Tear Resistance (Die C, ASTM D624) 400 +/- 50 pli 300 +/- 50 pli

Hardness (ASTM D2240) 90 +/- 5 Shore A 50 +/- 5 Shore D

Tests were performed with material and curing conditions at 75F and 50% relative humidity.

* + - 1. TRAFFIC COATINGS (SIKALASTIC 710 Lo-VOC/22 Lo-Mod HYBRID TRAFFIC SYSTEM)
				1. Pedestrian Traffic Coating: Sikalastic 710 Lo-VOC/22 Lo-Mod Hybrid Traffic System comprised of the following:

Primers :

Sikalastic Primer 1C fast curing PU primer.

Sikalastic FTP water-based epoxy primer.

Sikalastic FTP LoVOC 100% solids epoxy primer (as a standard primer and for recoat applications and elevated moisture content up to 6% by Tramex ).

Sikalastic PF Lo-VOC 100% solids epoxy primer (for rough and/or porous substrates).

Sikalastic MT 100% solids epoxy primer (for substrates with elevated moisture content up to 6 % by Tramex ).Sikalastic 710 Base one-component aromatic polyurethane base coat.

Sikalastic 710 Lo-VOC Base one-component aromatic polyurethane base coat.

Sikalastic 710 Lo-VOC Booster (optional)

Sikadur 22 Lo-Mod low-modulus, medium viscosity epoxy resin binder.

Sikalastic 700 ACL accelerator (optional).

Sikalastic 715 Lo-VOC Top aromatic, or 736 AL Lo-VOC aliphatic top coats (optional).

Sikalastic 715 Lo-VOC Booster (optional)

* + - * 1. Full Broadcast Method – Applied Total Dry Film Thickness Exclusive of Aggregate and Optional Top Coat:

Heavy Pedestrian Traffic: 43 mils.

* + - * 1. Aggregate: Clean, rounded, oven dried quartz sand with a minimum gradation of 16-30 mesh for vehicular traffic, and a minimum hardness of 6.5 per the Moh’s scale. Aggregate shall be supplied in pre-packaged bags and free of metallic or other impurities.
				2. Fabric Reinforcement: Sikalastic Flexitape Heavy woven nylon reinforcement.
				3. Base Coat: Typical Physical properties complying with the following.

Sikalastic 710 Lo-VOC Base

Viscosity 6500 +/- 3000 cps

Total Volume Solids (ASTM D2697) 89%

VOC Content (ASTM D2369) 93 g/l

Tensile Strength (ASTM D412) 1200 +/- 300 psi

Elongation at Break (ASTM D412) 450 +/- 50%

Tear Resistance (Die C, ASTM D624) 195 +/- 25 pli

Hardness (ASTM D2240) 75 +/- 5 Shore A

Tests were performed with material and curing conditions at 75°F and 50% relative humidity.

* + - * 1. Wear Coat: Typical Physical properties complying with the following.

Sikadur 22 Lo-Mod

Viscosity 2000 cps / 30 min

Total Volume Solids (ASTM D2697) 100%

VOC Content (ASTM D2369) 56 g/l

Tensile Strength (ASTM D638) 5,700 psi

Elongation at Break (ASTM D638) >30%

Hardness (ASTM D2240) 70 Shore D

Tests were performed with material and curing conditions at 75°F and 50% relative humidity.

* + - * 1. Aromatic Top Coat: Typical Physical properties complying with the following.

Sikalastic 715 Lo-VOC Top

Viscosity 4000 +/- 2000 cps

Total Volume Solids (ASTM D2697) 89%

VOC Content (ASTM D2369) 96 g/l

Tensile Strength (ASTM D412) 3400 +/- 300 psi

Elongation at Break (ASTM D412) 450 +/- 50%

Tear Resistance (Die C, ASTM D624) 350 +/- 50 pli

Hardness (ASTM D2240) 85 +/- 5 Shore A

Tests were performed with material and curing conditions at 75°F and 50% relative humidity.

* + - * 1. Aliphatic Top Coat: Typical Physical properties complying with the following.

Sikalastic 736 AL Lo-VOC

Viscosity 3500 +/- 700 cps

Total Volume Solids (ASTM D2697) 83%

VOC Content (ASTM D2369) 99 g/l

Tensile Strength (ASTM D412) 4000 +/- 300 psi

Elongation at Break (ASTM D412) 250 +/- 50%

Tear Resistance (Die C, ASTM D624) 400 +/- 50 pli

Hardness (ASTM D2240) 90 +/- 5 Shore A

Tests were performed with material and curing conditions at 75°F and 50% relative humidity.

* + - 1. TRAFFIC COATINGS (SIKALASTIC 720/745 TRAFFIC SYSTEM)
				1. Pedestrian Traffic Coating: Sikalastic 720/745 Traffic System comprised of the following:

Primers :

Sikalastic Primer 1C fast curing PU primer.

Sikalastic FTP water-based epoxy primer.

Sikalastic FTP LoVOC 100% solids epoxy primer (as a standard primer and for recoat applications and elevated moisture content up to 6% by Tramex ).

Sikalastic PF Lo-VOC 100% solids epoxy primer (for rough and/or porous substrates).

Sikalastic MT 100% solids epoxy primer (for substrates with elevated moisture content up to 6 % by Tramex ).Sikalastic 710 Base one-component aromatic polyurethane base coat.

Sikalastic 720 Base two-component aromatic polyurethane base coat.

Sikalastic 745 AL Top two-component aliphatic polyurethane top coat.

Sikalastic 736 AL Lo-VOC and 748 PA aliphatic top coats.

* + - * 1. Applied Total Dry Film Thickness Exclusive of Aggregate:

Pedestrian Traffic: 35 mils.

Heavy Pedestrian Traffic: 41 mils.

* + - * 1. Aggregate:

Standard Aggregate: Clean, rounded, oven dried quartz sand with a minimum gradation of 16-30 mesh or 20-40 mesh for pedestrian traffic, and a minimum hardness of 6.5 per the Moh’s scale. Aggregate shall be supplied in pre-packaged bags and free of metallic or other impurities.

Decorative Aggregate: UV-stable, ceramic-coated quartz aggregate in a standard or custom color blend. Intended for a full broadcast application where a clear sealcoat will be applied. Aggregate shall be supplied in pre-blended and packaged bags.

* + - * 1. Flakes:

Decorative Flakes: UV-stable, vinyl flakes in a standard or custom color blend. Intended for a partial or full broadcast application where a clear sealcoat will be applied. Flakes shall be supplied in pre-blended and packaged bags.

* + - * 1. Fabric Reinforcement: Sikalastic Flexitape Heavy woven nylon reinforcement.
				2. Base and Top Coats: Typical Physical properties complying with the following.

Sikalastic 720 Base 745 AL Top

Pot Life 10-15 minutes 20-30 minutes

Total Volume Solids (ASTM D2697) 95% 100%

VOC Content (ASTM D2369) 59 g/l 73.6 g/l

Tensile Strength (ASTM D412) 500 +/- 100 psi 3200 +/- 300 psi

Elongation at Break (ASTM D412) 800 +/- 50% 450 +/- 50%

Tear Resistance (Die C, ASTM D624) 300 +/- 25 pli 350 +/- 50 pli

Hardness (ASTM D2240) 80 +/- 5 Shore A 85 +/- 5 Shore A

Tests were performed with material and curing conditions at 75F and 50% relative humidity.

* + - * 1. Aliphatic Top Coat: Typical Physical properties complying with the following.

Sikalastic 736 AL Lo-VOC 748 PA

Viscosity 3500 +/- 700 cps 200 +/- 50 cps

Total Volume Solids (ASTM D2697) 83% 78%

VOC Content (ASTM D2369) 99 g/l 100 g/l

Tensile Strength (ASTM D412) 4000 +/- 300 psi 2500 +/- 200 psi

Elongation at Break (ASTM D412) 250 +/- 50% 100 +/- 25%.

Tear Resistance (Die C, ASTM D624) 400 +/- 50 pli 300 +/- 50 pli

Hardness (ASTM D2240) 90 +/- 5 Shore A 50 +/- 5 Shore D

Tests were performed with material and curing conditions at 75F and 50% relative humidity.

* + - 1. TRAFFIC COATINGS (SIKALASTIC 720/745 Textured TRAFFIC SYSTEM)
				1. Pedestrian Traffic Coating: Sikalastic 720/745 Textured Traffic System comprised of the following:

Primers :

Sikalastic Primer 1C fast curing PU primer.

Sikalastic FTP water-based epoxy primer.

Sikalastic FTP LoVOC 100% solids epoxy primer (as a standard primer and for recoat applications and elevated moisture content up to 6% by Tramex ).

Sikalastic PF Lo-VOC 100% solids epoxy primer (for rough and/or porous substrates).

Sikalastic MT 100% solids epoxy primer (for substrates with elevated moisture content up to 6 % by Tramex ).Sikalastic 710 Base one-component aromatic polyurethane base coat.

Sikalastic 720 Base two-component aromatic polyurethane base coat.

Sikalastic 745 Textured Top two-component aliphatic polyurethane top coat with integrated aggregate .

* + - * 1. Applied Total Dry Film Thickness Exclusive of Aggregate:

Pedestrian Traffic: 35 mils.

Heavy Pedestrian Traffic: 41 mils.

* + - * 1. Fabric Reinforcement: Sikalastic Flexitape Heavy woven nylon reinforcement.
				2. Base and Top Coats: Physical properties complying with the following.

Sikalastic 720 Base 745 Textured Top

Pot Life 10-15 minutes 20-30 minutes

Total Volume Solids (ASTM D2697) 95% 100%

VOC Content (ASTM D2369) 59 g/l 73.6 g/l

Tensile Strength (ASTM D412) 500 +/- 100 psi 3200 +/- 300 psi

Elongation at Break (ASTM D412) 800 +/- 50% 450 +/- 50%

Tear Resistance (Die C, ASTM D624) 300 +/- 25 pli 300 +/- 50 pli

Hardness (ASTM D2240) 80 +/- 5 Shore A 85 +/- 5 Shore A

Tests were performed with material and curing conditions at 75F and 50% relative humidity.

* + - 1. TRAFFIC COATINGS (SIKALASTIC 720/22 Lo-Mod HYBRID TRAFFIC SYSTEM)
				1. Pedestrian Traffic Coating: Sikalastic 720/22 Lo-Mod Hybrid Traffic System comprised of the following:

Primers :

Sikalastic Primer 1C fast curing PU primer.

Sikalastic FTP water-based epoxy primer.

Sikalastic FTP LoVOC 100% solids epoxy primer (as a standard primer and for recoat applications and elevated moisture content up to 6% by Tramex ).

Sikalastic PF Lo-VOC 100% solids epoxy primer (for rough and/or porous substrates).

Sikalastic MT 100% solids epoxy primer (for substrates with elevated moisture content up to 6 % by Tramex ).Sikalastic 710 Base one-component aromatic polyurethane base coat.

Sikalastic 720 Base two-component aromatic polyurethane base coat.

Sikadur 22 Lo-Mod low-modulus, medium viscosity epoxy resin binder.

Sikalastic 745 aliphatic top coat (optional).

* + - * 1. Full Broadcast Method – Applied Total Dry Film Thickness Exclusive of Aggregate and Optional Top Coat:

Heavy Pedestrian Traffic: 43 mils.

* + - * 1. Aggregate: Clean, rounded, oven dried quartz sand with a minimum gradation of 16-30 mesh for vehicular traffic, and a minimum hardness of 6.5 per the Moh’s scale. Aggregate shall be supplied in pre-packaged bags and free of metallic or other impurities.
				2. Fabric Reinforcement: Sikalastic Flexitape Heavy woven nylon reinforcement.
				3. Base Coat: Physical properties complying with the following.

Sikalastic 720 Base

Pot Life 10-15 minutes

Total Volume Solids (ASTM D2697) 95%

VOC Content (ASTM D2369) 59 g/l

Tensile Strength (ASTM D412) 500 +/- 100 psi

Elongation at Break (ASTM D412) 800 +/- 50%

Tear Resistance (Die C, ASTM D624) 300 +/- 25 pli

Hardness (ASTM D2240) 80 +/- 5 Shore A

Tests were performed with material and curing conditions at 75°F and 50% relative humidity.

* + - * 1. Wear Coat: Physical properties complying with the following.

Sikadur 22 Lo-Mod

Viscosity 2000 cps / 30 min

Total Volume Solids (ASTM D2697) 100%

VOC Content (ASTM D2369) 56 g/l

Tensile Strength (ASTM D638) 5,700 psi

Elongation at Break (ASTM D638) >30%

Hardness (ASTM D2240) 70 Shore D

Tests were performed with material and curing conditions at 75°F and 50% relative humidity.

* + - * 1. Aliphatic Top Coat: Physical properties complying with the following.

Sikalastic 745 AL Top

Pot Life 20-30 minutes

Total Volume Solids (ASTM D2697) 100%

VOC Content (ASTM D2369) 0 g/l

Tensile Strength (ASTM D412) 3200 +/- 300 psi

Elongation at Break (ASTM D412) 450 +/- 50%

Tear Resistance (Die C, ASTM D624) 350 +/- 50 pli

Hardness (ASTM D2240) 85 +/- 5 Shore A

Tests were performed with material and curing conditions at 75°F and 50% relative humidity.

* + - 1. TRAFFIC COATINGS (SIKALASTIC 390/391/395 TRAFFIC SYSTEM)
				1. Pedestrian Traffic Coating: Sikalastic 390/391/395 Traffic System comprised of the following:

Primers :

Sikalastic Primer 1C fast curing PU primer.

Sikalastic FTP water-based epoxy primer.

Sikalastic FTP LoVOC 100% solids epoxy primer (as a standard primer and for recoat applications and elevated moisture content up to 6% by Tramex ).

Sikalastic PF Lo-VOC 100% solids epoxy primer (for rough and/or porous substrates).

Sikalastic MT 100% solids epoxy primer (for substrates with elevated moisture content up to 6 % by Tramex ).Sikalastic 710 Base one-component aromatic polyurethane base coat.

Sikalastic 390 two-component aromatic polyurethane base coat.

Sikalastic 391 two-component aromatic polyurethane interior top coat and intermediate wear coat.

Sikalastic 395 two-component aliphatic polyurethane top coat.

Sikalastic 748 PA aliphatic top coat.

* + - * 1. Applied Total Dry Film Thickness Exclusive of Aggregate:

Light Pedestrian Traffic: 35 mils.

Heavy Pedestrian Traffic: 40 mils.

* + - * 1. Aggregate:

Standard Aggregate: Clean, rounded, oven dried quartz sand with a minimum gradation of 16-30 mesh or 20-40 mesh for pedestrian traffic, and a minimum hardness of 6.5 per the Moh’s scale. Aggregate shall be supplied in pre-packaged bags and free of metallic or other impurities.

Decorative Aggregate: UV-stable, ceramic-coated quartz aggregate in a standard or custom color blend. Intended for a full broadcast application where a clear sealcoat will be applied. Aggregate shall be supplied in pre-blended and packaged bags.

* + - * 1. Flakes:

Decorative Flakes: UV-stable, vinyl flakes in a standard or custom color blend. Intended for a partial or full broadcast application where a clear sealcoat will be applied. Flakes shall be supplied in pre-blended and packaged bags.

* + - * 1. Fabric Reinforcement: Sikalastic Flexitape Heavy woven nylon reinforcement.
				2. Base Coat: Typical Physical properties complying with the following.

Sikalastic 390

Pot Life 15-20 minutes

Total Volume Solids (ASTM D2697) 100%

VOC Content (ASTM D2369) <10 g/l

Tensile Strength (ASTM D412) 1,320 psi

Elongation at Break (ASTM D412) 435%

Tear Resistance (Die C, ASTM D624) 218 pli

Hardness (ASTM D2240) 80 +/- 5 Shore A

Tests were performed with material and curing conditions at 75°F and 50% relative humidity.

* + - * 1. Aromatic Top Coat: Physical properties complying with the following.

Sikalastic 391

Pot Life 35-45 minutes

Total Volume Solids (ASTM D2697) 100%

VOC Content (ASTM D2369) <10 g/l

Tensile Strength (ASTM D412) 595 psi

Elongation at Break (ASTM D412) 205%

Tear Resistance (Die C, ASTM D624) 396 pli

Hardness (ASTM D2240) 80 +/- 5 Shore A

Tests were performed with material and curing conditions at 75°F and 50% relative humidity.

* + - * 1. Aliphatic Top Coats: Typical Physical properties complying with the following.

Sikalastic 395 748 PA

Viscosity N/A 200 +/- 50 cps

Total Volume Solids (ASTM D2697) 100% 78%

VOC Content (ASTM D2369) <10 g/l 100 g/l

Tensile Strength (ASTM D412) 2500 psi 2500 +/- 200 psi

Elongation at Break (ASTM D412) 400% 100 +/- 25%.

Tear Resistance (Die C, ASTM D624) 79 pli 300 +/- 50 pli

Hardness (ASTM D2240) 85 +/- 5 Shore A 50 +/- 5 Shore D

Tests were performed with material and curing conditions at 75F and 50% relative humidity.

* + - 1. TRAFFIC COATINGS (SIKALASTIC 390/22 Lo-Mod HYBRID TRAFFIC SYSTEM)
				1. Pedestrian Traffic Coating: Sikalastic 390/22 Lo-Mod Hybrid Traffic System comprised of the following:

Primers :

Sikalastic Primer 1C fast curing PU primer.

Sikalastic FTP water-based epoxy primer.

Sikalastic FTP LoVOC 100% solids epoxy primer (as a standard primer and for recoat applications and elevated moisture content up to 6% by Tramex ).

Sikalastic PF Lo-VOC 100% solids epoxy primer (for rough and/or porous substrates).

Sikalastic MT 100% solids epoxy primer (for substrates with elevated moisture content up to 6 % by Tramex ).Sikalastic 710 Base one-component aromatic polyurethane base coat.

Sikalastic 390 Base two-component aromatic polyurethane base coat.

Sikadur 22 Lo-Mod low-modulus, medium viscosity epoxy resin binder.

Sikalastic 391 aromatic or 395 aliphatic top coats (optional).

* + - * 1. Full Broadcast Method – Applied Total Dry Film Thickness Exclusive of Aggregate and Optional Top Coat:

Heavy Pedestrian Traffic: 40 mils.

* + - * 1. Aggregate: Clean, rounded, oven dried quartz sand with a minimum gradation of 16-30 mesh for vehicular traffic, and a minimum hardness of 6.5 per the Moh’s scale. Aggregate shall be supplied in pre-packaged bags and free of metallic or other impurities.
				2. Fabric Reinforcement: Sikalastic Flexitape Heavy woven nylon reinforcement.
				3. Base Coat: Typical Physical properties complying with the following.

Sikalastic 390

Pot Life 15-20 minutes

Total Volume Solids (ASTM D2697) 100%

VOC Content (ASTM D2369) <10 g/l

Tensile Strength (ASTM D412) 1,320 psi

Elongation at Break (ASTM D412) 435%

Tear Resistance (Die C, ASTM D624) 218 pli

Hardness (ASTM D2240) 80 +/- 5 Shore A

Tests were performed with material and curing conditions at 75°F and 50% relative humidity.

* + - * 1. Wear Coat: Typical Physical properties complying with the following.

Sikadur 22 Lo-Mod

Viscosity 2000 cps / 30 min

Total Volume Solids (ASTM D2697) 100%

VOC Content (ASTM D2369) 56 g/l

Tensile Strength (ASTM D638) 5,700 psi

Elongation at Break (ASTM D638) >30%

Hardness (ASTM D2240) 70 Shore D

Tests were performed with material and curing conditions at 75°F and 50% relative humidity.

* + - * 1. Aromatic Top Coat: Typical Physical properties complying with the following.

Sikalastic 391

Pot Life 35-45 minutes

Total Volume Solids (ASTM D2697) 100%

VOC Content (ASTM D2369) <10 g/l

Tensile Strength (ASTM D412) 595 psi

Elongation at Break (ASTM D412) 205%

Tear Resistance (Die C, ASTM D624) 396 pli

Hardness (ASTM D2240) 80 +/- 5 Shore A

Tests were performed with material and curing conditions at 75°F and 50% relative humidity.

* + - * 1. Aliphatic Top Coat: Typical Physical properties complying with the following.

Sikalastic 395

Total Volume Solids (ASTM D2697) 100%

VOC Content (ASTM D2369) <10 g/l

Tensile Strength (ASTM D412) 2500 psi

Elongation at Break (ASTM D412) 400%

Tear Resistance (Die C, ASTM D624) 79 pli

Hardness (ASTM D2240) 85 +/- 5 Shore A

Tests were performed with material and curing conditions at 75°F and 50% relative humidity.

1. EXECUTION
	* + 1. EXAMINATION
				1. Verify that surfaces and conditions are ready to accept the Work of this section. Notify Architect in writing of any discrepancies. Commencement of the Work in an area shall mean Installer’s acceptance of the substrate.
			2. PREPARATION
				1. Substrates shall be clean, dry, sound and free of surface contaminants, with an open texture. Remove all traces of dust, laitance, grease, oils, curing compounds, form release agents and foreign particles by mechanical means, such as milling, scarifying, or shotblasting, as acceptable to the Architect. Blow surface free of dust using compressed air line-equipped with an oil trap. All projections, depressions and rough spots should be dressed off to achieve a level surface prior to the application.
				2. Concrete shall be cleaned and prepared to achieve a laitance and contaminant free, open textured surface by blast cleaning or equivalent mechanical means (CSP 3-4 per ICRI guidelines).
				3. Plywood shall be clean and smooth, APA and exterior grade, not less than 1/2 inch thick, and spaced and supported according to APA guidelines. Seams should be sealed with Sikaflex 2c or 1a and detailed and may need imbedded fabric reinforcement.
				4. Metal shall be thoroughly cleaned by grinding or blast cleaning.
			3. PRIMING
				1. Concrete (<4% moisture content by weight, measured with Tramex Concrete Moisture Encounter Meter) and Plywood:

For systems requiring primer, apply Sikalastic Primer at 280 sf/gal or Sikalastic FTP primer at 300 sf/gal with a flat squeegee or roller and work well into the substrate to insure adequate penetration and sealing. Puddles are to be avoided.

Refer to data sheet for more detailed information, or consult Sika for other primer options.

Sikalastic Primer - No mixing required. Apply product using using phenolic resin core roller or flat squeegee and backroll.

Allow primer to cure a minimum of 45 minutes at 70°F and 50% RH or until tack free before applying base coat.

Sikalastic FTP - premix both components. Part “B” is dark olive green in color and may appear black in the container. Sikalastic FTP, Part “A” is light amber in color.

Add the 1 gallon of Sikalastic FTP, Part “A” to the 1.25 gallons of Part “B” in the short filled Part “B” pail. Mix thoroughly with a mechanical mixer (Jiffy) for 3 minutes.

This mixture will appear as a light olive green color.

Slowly add 1.25 gallons of potable water to the mixture under agitation.

Mix for an additional 2 minutes until the mixture is fully dispersed.

Fully dispersed material will appear as light green in color.

Allow primer to cure a minimum of 3-4 hours at 70°F and 50% RH or until tack free before applying base coat.

* + - * 1. Concrete (<5% moisture content by weight, measured with Tramex Concrete Moisture Encounter Meter):

For concrete substrates with 5% maximum moisture content by weight, apply Sikalastic PF Lo-VOC primer at 200 sf/gal. with a flat squeegee or roller and work well into the substrate to insure adequate penetration and sealing. Puddles are to be avoided.

Refer to data sheet for more detailed information, or consult Sika for other primer options.

Premix both components. Sikalastic PF Lo-VOC Primer, Part “A” is white in color. Sikalastic PF Primer, Part “B” is black in color.

In a separate mixing vessel, add the Sikalastic PF Lo-VOC Primer, Part “B” to the Sikalastic PF Lo-VOC Part “A”. Mix thoroughly with a mechanical mixer (Jiffy) for 3 minutes.

This mixture will appear as a grey color.

Allow primer to cure a minimum of 6 hours at 70°F and 50% RH or until tack free before applying second primer or base coat.

* + - * 1. Concrete (4% to 6% moisture content by weight, measured with Tramex Concrete Moisture Encounter Meter):

For concrete substrates with 5% maximum moisture content by weight, apply Sikalastic MT primer at 175 sf/gal. with a flat squeegee or roller and work well into the substrate to insure adequate penetration and sealing. Puddles are to be avoided.

For concrete substrates with >5% up to 6% maximum moisture content by weight, apply a second coat of Sikalastic MT primer at 175 sf/gal.

Refer to data sheet for more detailed information, or consult Sika for other primer options.

Premix both components. Sikalastic MT Primer, Part “A” is red in color. Sikalastic MT Primer, Part “B” is light amber in color.

Add the 1.5 gallon of Sikalastic MT Primer, Part “B” to the 3 gallons of Part “A” in the short filled Part “A” pail. Mix thoroughly with a mechanical mixer (Jiffy) for 3 minutes.

This mixture will appear as a red transparent color.

Allow primer to cure a minimum of 12 hours at 70°F and 50% RH or until tack free before applying second primer or base coat.

For concrete substrates with 5% maximum moisture content by weight, apply Sikalastic FTP LoVOC primer at 200 sf/gal. with a flat squeegee or roller and work well into the substrate to insure adequate penetration and sealing. Puddles are to be avoided.

For concrete substrates with >5% up to 6% maximum moisture content by weight, apply a second coat of Sikalastic FTP LoVOC primer at 200 sf/gal.

Premix both components.

Add the 5 gallon of Sikalastic FTP LoVOC Primer, Part “B” to the 10 gallons of Part “A” . Mix thoroughly with a mechanical mixer (Jiffy) for 3 minutes.

This mixture will appear as a green transparent color.

Allow primer to cure a minimum of 12 hours at 70°F and 50% RH or until tack free before applying second primer or base coat.

* + - * 1. Metal: Consult manufacturer for selection of primer.
			1. DETAILING
				1. Non-Structural Cracks up to 1/16 inch: Apply a detail coat of Sikalastic 710 Base at 32 mils wet, Sikalastic 710 NP Base at 32 mils wet , Sikalastic 710 Lo-VOC Base at 26 mils wet, Sikalastic 715 Lo-VOC Top with Sikalastic 715 Lo-VOC Booster at 26 mils wet, Sikalastic 720 Base at 23 mils wet, or Sikalastic 390 at 30 mils wet, 4 inches wide, centered over the crack. Allow to become tack free before overcoating.
				2. Cracks and Joints over 1/16 inch up to 1 inch: Rout and seal with Sikaflex 2c or 1a sealant and allow to skin over and cure. Apply a detail coat of Sikalastic 710 Base at 32 mils wet, Sikalastic 710 NP Base , Sikalastic 710 Lo-VOC Base at 26 mils wet, Sikalastic 715 Lo-VOC Top with Sikalastic 715 Lo-VOC Booster at 26 mils wet, Sikalastic 720 Base at 23 mils wet, or Sikalastic 390 at 30 mils wet, 4 inches wide, centered over crack. Allow to become tack free before overcoating.
				3. Fabric Reinforcement: An optional 3” or 6” wide Sikalastic Flexitape Heavy fabric strip may be embedded within the base coat. Flexitape width shall be chosen such that a minimum of 1” tape is embedded on either side of the crack/joint. Apply additional coating as required to fully embed the Flexitape in the coating.
				4. Joints over 1 inch: Treat as expansion joints and brought up through the Sikalastic Traffic System and sealed with Sikaflex 2c or 1a sealant.
			2. BASE COAT
				1. Sikalastic 710 Base:

Thoroughly mix Sikalastic 710 Base using a mechanical mixer (Jiffy) at slow speeds until a homogenous mixture and color is obtained. Use care not to allow the entrapment of air into the mixture. Apply at the recommended coverage rate of 32 mils wet, using a 3/16” notched squeegee or trowel and backroll using a phenolic resin core roller. Extend base coat over entire area including previously detailed cracks and control joints. Allow coating to cure a minimum of 16 hours at 70°F and 50% RH or until tack free before top coating.

To speed cure time particularly in cold weather condition, Sikalastic 700 ACL may be added to Sikalastic 710 Base. Mix thoroughly prior to application. Add a maximum of 1 quart to 5 gallons (or 1:20 ratio), and only to material that will be applied within 2-3 hours. Allow coating to cure a minimum of 12 hours at 70°F and 50% RH; base coat must be tack free before overcoating.

* + - * 1. Sikalastic 710 Lo-VOC Base:

Thoroughly mix Sikalastic 710 Lo-VOC Base using a mechanical mixer (Jiffy) at slow speeds until a homogenous mixture and color is obtained. Add Sikalastic 710 Base Lo-VOC Booster (if required) into premixed coating and continue mixing until homogenous mixture and color is obtained (typically 3 minutes). Add a maximum of 1 quart to 4.75 gallons (or 1:19 ratio) and only to material that will be applied in the next hour. Use care not to allow the entrapment of air into the mixture. Apply at the recommended coverage rate of 26 mils wet, using a 1/4” notched squeegee or trowel and backroll using a phenolic resin core roller. Extend base coat over entire area including previously detailed cracks and control joints. Allow coating to cure a minimum of 16 hours (6 hours with Booster) at 70°F and 50% RH or until tack free before top coating.

* + - * 1. Sikalastic 710 NP Base:

Thoroughly mix Sikalastic 710 NP Base using a mechanical mixer (Jiffy) at slow speeds until a homogenous mixture and color is obtained. Use care not to allow the entrapment of air into the mixture. Apply at the recommended coverage rate of 32 mils wet, using a 3/16” notched squeegee or trowel and backroll using a phenolic resin core roller. Extend base coat over entire area including previously detailed cracks and control joints. Allow coating to cure a minimum of 16 hours at 70°F and 50% RH or until tack free before top coating.

* + - * 1. Sikalastic 715 Lo-VOC with Sikalastic 715 Lo-VOC Booster:

Thoroughly mix Sikalastic 715 Lo-VOC using a mechanical mixer (Jiffy) at slow speeds until a homogenous mixture and color is obtained. Add Sikalastic 715 Lo-VOC Booster into premixed coating and continue mixing until homogenous mixture and color is obtained (typically 3 minutes). Add a maximum of 1 quart to 4.75 gallons (or 1:19 ratio) and only to material that will be applied in the next hour. Use care not to allow the entrapment of air into the mixture.

Apply at the recommended coverage rate of 26 mils wet, using a 1/4” notched squeegee or trowel and backroll using a phenolic resin core roller. Extend base coat over entire area including previously detailed cracks and control joints. Allow coating to cure a minimum of 6 hours at 70°F and 50% RH or until tack free before top coating.

* + - * 1. Sikalastic 720 Base:

Premix Sikalastic 720 Base Part A and Part B using a mechanical mixer (Jiffy) at slow speeds to obtain uniform color, making sure to scrape the solids from the bottom and sides of the pails. Do not break down kits into smaller quantities; portions are premeasured.

Pour Part B into Part A slowly and while mixing, and scrape the sides of the container. Mix the combined materials thoroughly until a homogenous mixture and uniform color is obtained (typically 3 minutes). Use care not to allow the entrapment of air into the mixture.

Apply at the recommended coverage rate of 23 mils wet, using a 3/16” notched squeegee or trowel and backroll using a phenolic resin core roller. Extend base coat over entire area including previously detailed cracks and control joints.

Allow coating to cure a minimum of 3-4 hours at 70°F and 50% RH; base coat must be tack free before overcoating.

* + - * 1. Sikalastic 390 Base:

Premix Sikalastic 390 Base Part A and Part B using a mechanical mixer (Jiffy) at slow speeds to obtain uniform color, making sure to scrape the solids from the bottom and sides of the pails. Do not break down kits into smaller quantities; portions are premeasured.

Pour Part B into Part A slowly and while mixing, and scrape the sides of the container. Mix the combined materials thoroughly until a homogenous mixture and uniform color is obtained (typically 3 minutes). Use care not to allow the entrapment of air into the mixture.

Apply at the recommended coverage rate of 20 mils wet, using a 3/16” notched squeegee or trowel and backroll using a phenolic resin core roller. Extend base coat over entire area including previously detailed cracks and control joints.

Allow coating to cure a minimum of 5-6 hours at 70°F and 50% RH; base coat must be tack free before overcoating.

* + - 1. INTERMEDIATE COAT
				1. Sikalastic 715 (seed and lock application):

For heavy pedestrian traffic applications only, thoroughly mix Sikalastic 715 using a mechanical mixer (Jiffy) at slow speeds until a homogenous mixture and color is obtained. Use care not to allow the entrapment of air into the mixture.

Apply at 11 mils wet, using a 3/16” notched squeegee and backroll using a phenolic resin core roller. Apply aggregate evenly seeded and distributed at 10-15 lbs. per 100 sf into the wet coating and backroll if required. Allow coating to cure a minimum of 16 hours at 70°F and 50% RH or until tack free between coats.

To speed cure time particularly in cold weather condition, Sikalastic 700 ACL may be added to Sikalastic 715 . Mix thoroughly prior to application. Add a maximum of 1 quart to 5 gallons (or 1:20 ratio), and only to material that will be applied within 2-3 hours. Allow coating to cure a minimum of 8 hours at 70°F and 50% RH or until tack free before top coating.

* + - * 1. Sikalastic 715 Lo-VOC (seed and lock application):

For heavy pedestrian traffic applications only, thoroughly mix Sikalastic 715 Lo-VOC using a mechanical mixer (Jiffy) at slow speeds until a homogenous mixture and color is obtained.

Add Sikalastic 715 Lo-VOC Booster (if required) into premixed coating and continue mixing until homogenous mixture and color is obtained (typically 3 minutes). Add a maximum of 1 quart to 4.75 gallons (or 1:19 ratio) and only to material that will be applied in the next hour. Use care not to allow the entrapment of air into the mixture.

Apply at 9 mils wet, using a 3/16” notched squeegee and backroll using a phenolic resin core roller. Apply aggregate evenly seeded and distributed at 10-15 lbs. per 100 sf into the wet coating. Allow coating to cure a minimum of 16 hours (6 hours with Booster) at 70°F and 50% RH or until tack free between coats.

* + - * 1. Sikalastic 745 AL :

Not required.

* + - * 1. Sikalastic 391:

Not required.

* + - 1. TOP COAT
				1. Sikalastic 715 , Sikalastic 735 AL, Sikalastic 736 AL Lo-VOC:

Thoroughly mix Sikalastic 715 , Sikalastic 735 AL, or Sikalastic 736 AL Lo-VOC using a mechanical mixer (Jiffy) at slow speeds until a homogenous mixture and color is obtained. Use care not to allow the entrapment of air into the mixture.

For light pedestrian traffic applications, apply at 14 mils wet (12 mils wet 736 AL Lo-VOC), using a notched squeegee and backroll using a phenolic resin core roller. Apply aggregate evenly seeded and distributed at 5-10 lbs. per 100 sf into the wet coating and backroll.

For heavy pedestrian traffic applications, apply at 16 mils wet (14 mils wet 736 AL Lo-VOC), using a notched squeegee and backroll using a phenolic resin core roller.

Allow coating to cure a minimum of 16 hours at 70°F and 50% RH or until tack free between coats. Allow a minimum of 72 hours before opening to pedestrian traffic.

To speed cure time particularly in cold weather condition, Sikalastic 700 ACL may be added to Sikalastic 715 , Sikalastic 735 AL, or Sikalastic 736 AL Lo-VOC. Mix thoroughly prior to application. Add a maximum of 1 quart to 5 gallons (or 1:20 ratio), and only to material that will be applied within 2-3 hours. Allow coating to cure a minimum of 8 hours at 70°F and 50% RH or until tack free before top coating. Allow a minimum of 48 hours before opening to vehicular traffic.

* + - * 1. Sikalastic 715 Lo-VOC Top:

Thoroughly mix Sikalastic 715 Lo-VOC using a mechanical mixer (Jiffy) at slow speeds until a homogenous mixture and color is obtained. Add Sikalastic 715 Lo-VOC Booster (if required) into premixed coating and continue mixing until homogenous mixture and color is obtained (typically 3 minutes). Add a maximum of 1 quart to 4.75 gallons (or 1:19 ratio) and only to material that will be applied in the next hour. Use care not to allow the entrapment of air into the mixture.

For light pedestrian traffic applications, apply at 11 mils wet, using a notched squeegee and backroll using a phenolic resin core roller. Apply aggregate evenly seeded and distributed at 5-10 lbs. per 100 sf into the wet coating and backroll.

For heavy pedestrian traffic applications, apply at 13 mils wet, using a notched squeegee and backroll using a phenolic resin core roller.

Allow coating to cure a minimum of 16 hours (6 hours with Booster) at 70°F and 50% RH or until tack free between coats. Allow a minimum of 72 hours (36 hours with Booster) before opening to pedestrian traffic.

* + - * 1. Sikalastic 715 Textured:

Thoroughly mix for 3 minutes using a mechanical mixer (Jiffy) at slow speed until a homogenous mixture and uniform color is obtained . Make sure to scrape the solids and the aggregate from the bottom and sides of the pail. The aggregate should be evenly diffused in the resin. Use care not to allow the entrapment of air into the mixture.

Apply at the recommended coverage rate using a 1/8” or 1/16” notched squeegee or trowel, and backroll using nap roller 3/8” to uniformly backroll . The Top coat should be backrolled two times, one perpendicular to the other. Allow coating to cure a minimum of 4 hours at 70°F and 50% RH; coating must be tack free before overcoating.

Allow coating to cure a minimum of 16 hours at 70°F and 50% RH or until tack free between coats. Allow a minimum of 72 hours before opening to pedestrian traffic.

To speed cure time particularly in cold weather condition, Sikalastic 700 ACL may be added to Sikalastic 715 Textured . Mix thoroughly prior to application. Add a maximum of 1 quart to 5 gallons (or 1:20 ratio), and only to material that will be applied within 2-3 hours. Allow coating to cure a minimum of 8 hours at 70°F and 50% RH or until tack free before top coating. Allow a minimum of 48 hours before opening to vehicular traffic.

* + - * 1. Sikalastic 745 AL :

Premix Sikalastic 745 AL Part A and Part B using a mechanical mixer (Jiffy) at slow speeds to obtain uniform color, making sure to scrape the solids from the bottom and sides of the pails. Do not break down kits into smaller quantities; portions are premeasured.

Pour Part B into Part A slowly and while mixing, and scrape the sides of the container. Mix the combined materials thoroughly until a homogenous mixture and uniform color is obtained (typically 3 minutes). Use care not to allow the entrapment of air into the mixture.

For light pedestrian traffic applications, apply at 12 mils wet, using a notched squeegee and backroll using a phenolic resin core roller. Apply aggregate evenly seeded and distributed at 5-10 lbs. per 100 sf into the wet coating and backroll.

For heavy pedestrian traffic applications, apply at 18 mils wet, using a notched squeegee and backroll using a phenolic resin core roller. Apply aggregate evenly seeded and distributed at 10-20 lbs. per 100 sf into the wet coating and backroll.

Allow coating to cure a minimum of 3-4 hours at 70 degrees F and 50% RH or until tack free between coats, and a minimum of 36 hours before opening to vehicular traffic.

* + - * 1. Sikalastic 745 Textured :

Premix Sikalastic 745 Textured Part A using a mechanical mixer (Jiffy) at slow speeds to obtain uniform color and mixture, making sure to scrape the solids and the aggregate from the bottom and sides of the pail. The aggregate should be evenly diffused in the resin.

Pour part B into Part A slowly and while mixing scrape the side of the container. Mix the combined material thoroughly until a homogenous mixture and uniform color is obtained. Do not break down kits into smaller quantities; portions are premeasured.

Apply at the recommended coverage rate using 1/8”or 3/16” notched squeegee or trowel, and backroll using a phenolic resin core roller to uniformly backroll . The top coat should be backrolled two times , one perpendicular to the other.

Allow coating to cure a minimum of 3-4 hours at 70 degrees F and 50% RH or until tack free between coats, and a minimum of 36 hours before opening to vehicular traffic

* + - * 1. Sikalastic 391 and 395:

Premix Sikalastic 391 or Sikalastic 395 Part A and Part B using a mechanical mixer (Jiffy) at slow speeds to obtain uniform color, making sure to scrape the solids from the bottom and sides of the pails. Do not break down kits into smaller quantities; portions are premeasured.

Pour Part B into Part A slowly and while mixing, and scrape the sides of the container. Mix the combined materials thoroughly until a homogenous mixture and uniform color is obtained (typically 3 minutes). Use care not to allow the entrapment of air into the mixture.

For light pedestrian traffic applications, apply at 15 mils wet, using a notched squeegee and backroll using a phenolic resin core roller. Apply aggregate evenly seeded and distributed at 5-10 lbs. per 100 sf into the wet coating and backroll.

For heavy pedestrian traffic applications, apply at 20 mils wet, using a notched squeegee and backroll using a phenolic resin core roller. Apply aggregate evenly seeded and distributed at 10-20 lbs. per 100 sf into the wet coating and backroll.

Allow coating to cure a minimum of 10 hours at 70 degrees F and 50% RH or until tack free between coats, and a minimum of 48 hours before opening to vehicular traffic.

* + - 1. ALTERNATIVE DECORATIVE TOPCOATS
				1. Sikalastic 735 AL and Sikalastic 748 PA:

Apply decorative topcoats directly to cured Sikalastic 710 Base instead of Sikalastic 715.

Thoroughly mix Sikalastic 735 AL using a mechanical mixer (Jiffy) at slow speeds until a homogenous mixture and color is obtained. Use care not to allow the entrapment of air into the mixture.

Apply at 14 mils wet, using a notched squeegee and backroll using a phenolic resin core roller. For a decorative aggregate system, apply decorative aggregate in a full broadcast at the rate of 40-50 lbs./100 sf. For a decorative flake system, apply decorative flakes seeded or in a full broadcast at the rate of 2-5 lbs./100 sf. Allow to cure 16 hours at 70 degrees F and 50% RH or until tack free. Remove all loose aggregate and flakes once coating has cured.

Premix Sikalastic 748 PA Part A and Part B before combining. Add equal amounts of Part B to Part A while mixing using a mechanical mixer (Jiffy) at medium speed. Mix until a homogenous mixture and color is obtained (at least 3 minutes) and mix frequently during application to maintain uniform color and consistency. Scrape the sides of the container to ensure that no unmixed material remains and use care not to allow the entrapment of air into the mixture as this may result in pinhole blisters or shortened pot life.

Apply at the recommended coverage rate below, using a notched squeegee and backroll using a phenolic resin core roller. Apply at 13 mils wet to seal decorative aggregate, and at 9 mils wet to seal decorative flakes. Allow coating to cure 2-4 hours at 70 degrees F and 50% RH or until tack free, and 24-48 hours before opening to pedestrian traffic.

* + - * 1. Sikalastic 736 AL Lo-VOC and Sikalastic 748 PA:

Apply decorative topcoats directly to cured Sikalastic 720 Base/Sikalastic 710 Lo-VOC Base instead of Sikalastic 745 AL/Sikalastic 715 Lo-VOC.

Thoroughly mix Sikalastic 736 AL Lo-VOC using a mechanical mixer (Jiffy) at slow speeds until a homogenous mixture and color is obtained. Use care not to allow the entrapment of air into the mixture.

Apply at 12 mils wet, using a notched squeegee and backroll using a phenolic resin core roller. For a decorative aggregate system, apply decorative aggregate in a full broadcast at the rate of 40-50 lbs./100 sf. For a decorative flake system, apply decorative flakes seeded or in a full broadcast at the rate of 2-5 lbs./100 sf. Allow to cure 16 hours at 70 degrees F and 50% RH or until tack free. Remove all loose aggregate and flakes once coating has cured.

Premix Sikalastic 748 PA Part A and Part B before combining. Add equal amounts of Part B to Part A while mixing using a mechanical mixer (Jiffy) at medium speed. Mix until a homogenous mixture and color is obtained (at least 3 minutes) and mix frequently during application to maintain uniform color and consistency. Scrape the sides of the container to ensure that no unmixed material remains and use care not to allow the entrapment of air into the mixture as this may result in pinhole blisters or shortened pot life.

Apply at the recommended coverage rate below, using a notched squeegee and backroll using a phenolic resin core roller. Apply at 13 mils wet to seal decorative aggregate, and at 9 mils wet to seal decorative flakes. Allow coating to cure 2-4 hours at 70 degrees F and 50% RH or until tack free, and 24-48 hours before opening to pedestrian traffic.

* + - * 1. Sikalastic 395 and Sikalastic 748 PA:

Apply decorative topcoats directly to cured Sikalastic 390 Base.

Premix Sikalastic 395 Top Part A and Part B using a mechanical mixer (Jiffy) at slow speeds to obtain uniform color, making sure to scrape the solids from the bottom and sides of the pails. Do not break down kits into smaller quantities; portions are premeasured.

Pour Part B into Part A slowly and while mixing, and scrape the sides of the container. Mix the combined materials thoroughly until a homogenous mixture and uniform color is obtained (typically 3 minutes). Use care not to allow the entrapment of air into the mixture.

Apply at 12 mils wet, using a notched squeegee and backroll using a phenolic resin core roller. For a decorative aggregate system, apply decorative aggregate in a full broadcast at the rate of 40-50 lbs./100 sf. For a decorative flake system, apply decorative flakes seeded or in a full broadcast at the rate of 2-5 lbs./100 sf. Allow to cure 6 hours at 70 degrees F and 50% RH or until tack free. Remove all loose aggregate and flakes once coating has cured.

Premix Sikalastic 748 PA Part A and Part B before combining. Add equal amounts of Part B to Part A while mixing using a mechanical mixer (Jiffy) at medium speed. Mix until a homogenous mixture and color is obtained (at least 3 minutes) and mix frequently during application to maintain uniform color and consistency. Scrape the sides of the container to ensure that no unmixed material remains and use care not to allow the entrapment of air into the mixture as this may result in pinhole blisters or shortened pot life.

Apply at the recommended coverage rate below, using a notched squeegee and backroll using a phenolic resin core roller. Apply at 13 mils wet to seal decorative aggregate, and at 9 mils wet to seal decorative flakes. Allow coating to cure 2-4 hours at 70 degrees F and 50% RH or until tack free, and 24-48 hours before opening to pedestrian traffic.

* + - 1. hybrid EPOXY WEAR COAT
				1. Sikadur 22 Lo-Mod – Full Broadcast Method:

Premix Sikadur 22 Lo-Mod Part A and Part B using a mechanical mixer (Jiffy) at slow speeds to obtain uniform color, making sure to scrape the solids from the bottom and sides of the pails. Do not break down kits into smaller quantities; portions are premeasured.

Pour Part B into Part A slowly and while mixing, and scrape the sides of the container. Mix the combined materials thoroughly until a homogenous mixture and uniform color is obtained (typically 3 minutes). Use care not to allow the entrapment of air into the mixture.

Apply at the required application rate using a 3/16” or ¼” notched squeegee and backroll using a phenolic resin core roller. Application rate is 20 mils wet for heavy pedestrian traffic applications.

Apply aggregate 1.25 – 1.5 lbs. per sf into the wet coating. Slowly broadcast so the aggregate falls vertically into the binder making several passes, allow the binder to bleed through the sand before making the next pass. Cover completely before binder becomes tack free. Allow coating to cure a minimum of 8 hours at 70 degrees F and 50% RH or until tack free between coats. Remove all loose aggregate before top coating or opening to traffic. Allow a minimum of 8 hours before top coating. If no top coat is to be applied, allow a minimum of 24 hours (720 Base/710 Lo-VOC Base with Booster), 36 hours (390), or 48 hours (710 Base/710 Lo-VOC Base) before opening to vehicular traffic.

* + - * 1. Sikadur 22 Lo-Mod – Seed and Backroll Method:

Premix Sikadur 22 Lo-Mod Part A and Part B using a mechanical mixer (Jiffy) at slow speeds to obtain uniform color, making sure to scrape the solids from the bottom and sides of the pails. Do not break down kits into smaller quantities; portions are premeasured.

Pour Part B into Part A slowly and while mixing, and scrape the sides of the container. Mix the combined materials thoroughly until a homogenous mixture and uniform color is obtained (typically 3 minutes). Use care not to allow the entrapment of air into the mixture.

Apply at the required application rate using a 3/16” or ¼” notched squeegee and backroll using a phenolic resin core roller. Application rate is 16 mils wet for heavy pedestrian traffic applications.

Apply aggregate evenly seeded and distributed at 10-20 lbs. per 100 sf into the wet coating. Allow coating to cure a minimum of 8 hours at 70 degrees F and 50% RH or until tack free between coats. Remove all loose aggregate before top coating.

* + - 1. hybrid top coat (optional for full broadcast method, required for seed and backroll method)
				1. Sikalastic 715, 735 AL, and 736 AL Lo-VOC:

Full Broadcast Method – Apply over tack free Sikadur 22 Lo-Mod following removal of all loose aggregate. Apply at 23 mils wet, using a 3/16” notched squeegee and backroll using a phenolic resin core roller. Allow a minimum of 48 hours before opening to pedestrian traffic.

Seed and Backroll Method – Apply over tack free Sikadur 22 Lo-Mod following removal of all loose aggregate. Apply at 16 mils wet, using a 3/16” notched squeegee and backroll using a phenolic resin core roller. Allow a minimum of 48 hours before opening to pedestrian traffic.

* + - * 1. Sikalastic 715 Lo-VOC:

Full Broadcast Method – Apply over tack free Sikadur 22 Lo-Mod following removal of all loose aggregate. Apply at 21 mils wet, using a 3/16” notched squeegee and backroll using a phenolic resin core roller. Allow a minimum of 48 hours (24 hours with Booster) before opening to pedestrian traffic.

Seed and Backroll Method – Apply over tack free Sikadur 22 Lo-Mod following removal of all loose aggregate. Apply at 13 mils wet, using a 3/16” notched squeegee and backroll using a phenolic resin core roller. Allow a minimum of 48 hours (24 hours with Booster) before opening to pedestrian traffic.

* + - * 1. Sikalastic 745 AL:

Full Broadcast Method – Apply over tack free Sikadur 22 Lo-Mod following removal of all loose aggregate. Apply at 18 mils wet, using a 3/16” notched squeegee and backroll using a phenolic resin core roller. Allow a minimum of 24 hours before opening to pedestrian traffic.

Seed and Backroll Method – Apply over tack free Sikadur 22 Lo-Mod following removal of all loose aggregate. Apply at 12 mils wet, using a 3/16” notched squeegee and backroll using a phenolic resin core roller. Allow a minimum of 24 hours before opening to pedestrian traffic.

* + - * 1. Sikalastic 395:

Full Broadcast Method – Apply over tack free Sikadur 22 Lo-Mod following removal of all loose aggregate. Apply at 18 mils wet, using a 3/16” notched squeegee and backroll using a phenolic resin core roller. Allow a minimum of 24 hours before opening to pedestrian traffic.

Seed and Backroll Method – Apply over tack free Sikadur 22 Lo-Mod following removal of all loose aggregate. Apply at 12 mils wet, using a 3/16” notched squeegee and backroll using a phenolic resin core roller. Allow a minimum of 24 hours before opening to pedestrian traffic.

* + - 1. CLEANING
				1. Remove uncured materials from tools or other surfaces with an approved solvent. Remove cured materials by mechanical means.
				2. Leave finished work and work area in a neat, clean condition without evidence of spillovers onto adjacent areas.

END OF SECTION

The preceding specifications are provided by Sika Corporation as a guide for informational purposes only and are not intended to replace sound engineering practice and judgment and should not be relied upon for that purpose. **Sika Corporation makes no warranty of any kind, either express or implied, as to the accuracy, completeness or the contents of these guide specifications**. Sika Corporation assumes no liability with respect to the provision or use of these guide specifications, nor shall any legal relationship be created by, or arise from, the provision of such specifications **SIKA SHALL NOT BE RESPONSIBLE UNDER ANY LEGAL THEORY TO ANY THIRD PARTY FOR ANY DIRECT OR CONSEQUENTIAL DAMAGES OF ANY KIND ARISING FROM THE USE OF THESE GUIDE SPECIFICATIONS.** The specifier, architect, engineer or design professional or contractor for a particular project bears the sole responsibility for the preparation and approval of the specifications and determining their suitability for a particular project or application.

Prior to each use of any Sika product, the user must always read and follow the warnings and instructions on the product's most current Technical Data Sheet, product label and Material Safety Data Sheet which are available at www.sikausa.com or by calling (800) 933-7452. Nothing contained in any Sika materials relieves the user of the obligation to read and follow the warnings and instructions for each Sika product as set forth in the current Technical Data Sheet, product label and Material Safety Data Sheet prior to product use.