SECTION 033619 - PENETRATING REACTIVE CONCRETE STAIN

This Section specifies a water-based reactive chemical concrete stain incorporating Scofield’s LITHOCHROME Tintura Stain, manufactured by Sika Corporation. Tintura combines with cured concrete to produce unique translucent or opaque color effects.  An ideal product for exterior and interior floors not subject to abrasion or heavy traffic. Tintura is also suitable for use on vertical concrete surfaces such as walls and columns, and existing concrete surfaces.  This is a low VOC product meeting stringent air quality management regulations.

Refer to www.scofield.com for current Scofield Tech-Data Bulletins describing materials and installation requirements.  Customer service number is (800) 800-9900.

- GENERAL

      - SUMMARY

        - Section includes:

          - Water-based reactive stained concrete floor finish.

          - Sealer.

        - Related Sections:

- Edit to suit Project requirements.

          - Section 033000 “Cast-In-Place Concrete” for general concrete applications.

          - Section 079200 “Joint Sealants” for colored sealant installed in paving joints.

      - REFERENCES

        - ASTM International (ASTM):

          - ASTM C 171:  Standard Specification for Sheet Materials for Curing Concrete.

          - ASTM C 309:  Standard Specification for Liquid Membrane-Forming Compounds for Curing Concrete.

        - International Concrete Repair Institute (ICRI):

          - ICRI Technical Guidelines:  Series 300 - Concrete, Designation 310 - Surface Preparation.

      - SUBMITTALS

        - Product Data:  Manufacturer’s technical data, including Safety Data Sheet (SDS) and installation instructions, for each product specified.

- Include LEED submittal for credit Low-Emitting Materials: Interior Paints & Coatings if this project will be submitted for LEED certification.

        - LEED Documentation, Low-Emitting Materials: Interior Paints & Coatings:  Verification of VOC content.

        - Samples for Initial Selection:  Manufacturer’s color charts showing full range of colors available.

        - Qualification Data:  For manufacturer and Installer.

      - QUALITY ASSURANCE

        - Manufacturer Qualifications:  Minimum 10 years of documented experience producing the specified products.

        - Installer Qualifications:  Minimum 5 years of documented experience with work of similar scope and complexity required by this Project and acceptable to, or certified by, concrete stain manufacturer.

        - Regulatory Requirements:

- Code of Federal Regulations 40 CFR 59, Subpart D and EPA Test Method 24 establish VOC emissions standards and test protocols for architectural coatings.

          - Products to comply with United States Clean Air Act for maximum Volatile Organic compound (VOC) content as specified in this Section.

        - Material Source Limitations:  Obtain each specified material from the same source.

        - Notification:  Give a minimum 7 calendar days’ notice to manufacturer’s authorized field representative before date established for commencement of concrete stain work.

- For large projects or where color and appearance are critical, include provisions for a

- mockup to demonstrate finished appearance and workmanship standards.

        - Concrete Stain Mockups:

          - Construct a 10 foot by 10 foot mockup at location selected by Architect.

          - Provide individual mockups for each color required.

          - Construct mockup using materials, processes, and techniques required for the work, including curing procedures. Incorporate representative control, construction, and expansion joints according to Project requirements.  Installer for the work to construct mockup.

          - Mockup to be stained and sealed by the Installer who will actually perform the work for the Project.  Record the amount of chemical stain needed per square foot of application to establish coverage rates for the work.

          - Notify Architect and Owner a minimum of seven calendar days in advance of the date scheduled for each mockup construction.

          - Obtain the Architect’s and Owner’s acceptance of each mockup prior to commencement of the work.

          - Each mockup to remain until completion of the work to serve as a quality control standard for the work.  Provide suitable protections to preclude damage to mockup.

- Retain one the following two paragraphs.

          - Approved mockup may become part of the completed work if undisturbed at time of Substantial Completion.

          - Demolish and remove each mockup from site when directed.

      - DELIVERY, STORAGE, AND HANDLING

        - Deliver products in original factory unopened, undamaged packaging bearing identification of product, manufacturer, batch number, and expiration date as applicable.

        - Store products in a location protected from damage, construction activity, and adverse environmental conditions, and away from combustible materials and sources of heat, according to manufacturer’s printed instructions and current recommendations.

        - Handle products according to manufacturer’s printed instructions.

      - PROJECT CONDITIONS

        - Environmental Conditions:  Maintain an ambient temperature between 50 deg F and 90 deg F during application and at least 48 hours after application.  Do not proceed with exterior applications during rainy, foggy, or very humid weather.

      - PREINSTALLATION CONFERENCE

        - Seven calendar days prior to scheduled date of installation, conduct a meeting at Project site to discuss requirements, including application methods.  Attendees to include Architect, Owner, Contractor, Installer, and manufacturer’s authorized field representative.

- PRODUCTS

      - ACCEPTABLE MANUFACTURERS

        - Basis of Design:  Provide products specified herein manufactured by Sika Corporation.

      - MATERIALS

        - Water-Based Reactive Chemical Concrete Stain:  Penetrating reactive water-based staining product that chemically bonds to cured concrete or cementitious topping substrates to produce permanent translucent color effects.  Less than 100 g/L VOC content.

          - Product: “LITHOCHROME Tintura Stain, Sika Corporation.”

- Select color(s) to suit Project requirements. Refer to LITHOCHROME Tintura Color Selection Guide A-422 for full range of standard colors available.

          - Color(s): ____________________.

- Select sealing compound from available choices below, and to suit project requirements. Consult the sealer selection guide at www.scofield.com.

          - Sealers - choose from one of the following sealers:

            - SCOFIELD® Selectseal PlusTM , Sika Corporation

            - SCOFIELD® CureselTM 700 , Sika Corporation

            - SCOFIELD® CuresealTM 350 , Sika Corporation

            - SCOFIELD® Cureseal-WTM , Sika Corporation

- EXECUTION

      - EXAMINATION

        - Examine areas and conditions under which the concrete stain work will be performed and identify conditions detrimental to the proper and timely completion of the work.  Do not proceed until unsatisfactory conditions have been corrected.

      - PREPARATION

        - New Concrete:  Comply with the following:

          - Newly placed concrete to sufficiently cure for concrete to become reactive. Minimum cure time is 28 days.

          - Do not use liquid curing materials.  Cure concrete flatwork with new, unwrinkled, non-staining, high quality curing paper complying with ASTM C 171.  Do not overlap curing paper.

        - Surface Preparation for New or Existing Concrete:

          - Concrete surfaces should be completely penetrable before applying the initial application of chemical stain. The surface of the concrete should be lightly mechanically abraded to remove weak cement paste and contaminants. The final surface preparation should approximate a Concrete Surface Profile of 1, (CSP1 as designated by the International Concrete Repair Institute, Alexandria, Virginia). Methods for mechanical abrasion include:

            - Pressure Washing: Use a pressure washer equipped with a fan tip and rated for a minimum pressure capability of 4000 psi.

            - Scrubbing with a rotary floor machine with a Mal-Grit Brush from the Malish Corporation.

            - Light sanding of the surface.

- Surfaces should be tested to receive stain by spotting with water.  Water should immediately darken the substrate and be readily absorbed.  If water beads and does not penetrate or only penetrates in some areas, perform additional surface preparation and testing.  On denser concrete floors, sand lightly to open up surfaces.  Retest and continue surface preparation until water spots immediately darken and uniformly penetrate concrete surfaces.

          - Rinse concrete substrates until rinse water is completely clean.

- Retain the following paragraph if decorative scoring is a design element.

        - Scoring: Score decorative jointing in concrete surfaces 1/8 inch deep with diamond blades. Rinse until water is completely clean.

        - Completed preparation to result in concrete surfaces that are uniformly slip-resistant and profiled to meet a Concrete Surface Preparation (CSP) of 1-2 according to referenced ICRI guidelines.

      - CONCRETE STAIN APPLICATION

        - Protect surrounding areas, landscaping, and adjacent surfaces from overspray, runoff, and tracking.  Divide surfaces into small work sections using walls, joint lines, or other stationary breaks as natural stopping points.

        - Apply concrete stains full strength (undiluted) at the coverage rate recommended by the manufacturer and use application equipment according to the concrete stain manufacturer’s printed instructions.  Note the color of the liquid chemical stain will not be the final color produced on the concrete substrate.

          - Thoroughly power mix concrete stain base and tint materials immediately prior to use.  For mixing stain materials, use an acceptable metal blade mixer.

        - Apply water-based reactive stain to substrates with an airless sprayer or High Volume Low Pressure (HVLP) sprayer, with a maintained and overlap controlled wet edge.  A roller may also be used to apply material. If an airless sprayer or HVLC sprayer is used, the material may be manipulated mechanically to create a variegated appearance similar to that of an acid stain. If a roller is used an opaque monochromatic appearance will result.

          - Airless Sprayer:  1500 to 2500 psi variable outlet fluid pressure.  0.013 to 0.018 inch tip.

          - HVLP Sprayer:  5 to 40 psi spray pressure capability.

        - Reaction time will depend of wind conditions, temperature, and humidity level.

        - If required, apply a second coat after first coat has sufficiently dried and can be walked on without damage; normally two to four hours after application depending on temperature and humidity.  Apply a third coat, if required, not less than two to four hours after the second coat application.

        - On vertical surfaces, start spray applications of reactive stain at the bottom and proceed upward.  Apply stain material in light coats while maintaining a wet edge to ensue penetration into the surface.

      - SEALER APPLICATION

        - Concrete substrate must be completely dry.

        - After the final penetrating stain application has dried sufficiently, normally 8 to 24 hours at 75 degrees F and 50 percent relative humidity, remove all contaminants from surfaces by dry mopping if required.

        - Apply sealer according the sealer manufacturer’s printed instructions at a rate of 300 to 500 square feet per gallon per coat, maintaining a wet edge at all times.  Two coats are required.  Maintain a wet edge at all times.

        - Allow sealer to completely dry before applying additional coats.

        - Apply second coat of sealer at 90 degrees to the direction of the first coat using the same application method and rates.

        - Seal horizontal joints in areas subject to pedestrian or vehicular traffic.

      - PROTECTION

- A.     The General Contractor is responsible for using Temporary Floor Protection throughout          the project to safeguard the surface quality of concrete slabs before and after application of decorative finishes or installations of other materials.

        - All concrete floors that will be not be covered by other materials will be protected throughout the project. The concrete slab must be treated as a finished floor at all times during construction.

        - Temporary Floor Protection will be removed only while finish work to the concrete is being performed and will be replaced after the final finish has cured sufficiently.

        - Temporary Floor Protection will be SCOFIELD Proguard Duracover, manufactured by Sika Corporation. Seaming of the temporary floor protection will be performed with SCOFIELD Proguard Heavy Duty Seaming Tape.  Both products will be installed following the manufacturer’s published installation procedures.

        - DO NOT APPLY THE HEAVY DUTY SEAMING TAPE TO BARE OR FINISHED FLOORS OR WALL SURFACES AT ANY TIME. IT WILL PERMANENTLY DAMAGE THE FLOOR

        - No substitutions will be allowed.

      - MAINTENANCE

        - Maintain water-based reactive stained and sealed floors by sweeping. Clean spills when they occur and rinse dirt off with water.  Wet-clean heavily soiled areas by mopping or by scrubbing with a rotary floor machine equipped with a scrubbing brush and a suitable, high quality commercial detergent.  Maintain interior floors that require polishing by using a compatible, premium-grade, emulsion-type, commercial floor polish, according to manufacturer’s printed instructions and safety requirements.

END OF SECTION 033619

© Sika Corporation