SIKA SPECIFICATION NOTE: This guide specification is provided in CSI Format for use by design professionals for individual construction projects. Modify the text based on your project requirements, and delete products not required. Questions? Call 800-933-SIKA.

SIKA SPECIFICATION NOTE: This guide specification includes test methods, materials and installation procedures for Sikalastic Cold Fluid Applied Polyurea Hybrid Protected Roofing/Waterproofing Membrane System or as an Exposed Roofing/Waterproofing Membrane System. Sikalastic is a fully bonded, elastomeric waterproofing membrane designed for use over most common construction surfaces including concrete, plywood sheathing, metal substrates and/or modified bitumen roofing membranes.

SECTION 07 55 56

FLUID-APPLIED PROTECTED MEMBRANE ROOFING/Waterproofing

OR

Section 07 56 00

FLUID-APPLIED MEMBRANE ROOFING/Waterproofing

1. GENERAL
	* + 1. RELATED DOCUMENTS
				1. Drawings and general provisions of the Contract, including General and Supplementary Conditions and Division 01 Specification Sections, apply to this Section.
			2. SUMMARY
				1. Provide a protected cold-fluid-applied polyurea hybrid roofing/waterproofing system on structural concrete, plywood sheathing, metal or other approved substrates.

Work includes substrate preparation.

Work includes bridging and sealing air leakage and water intrusion pathways and gaps including connections of the walls to the roof air barrier, and penetrations of the building envelope including piping, conduit, ducts and similar items.

* + - * 1. Related Work: The following items are not included in this Section and are specified under the designated Sections:

Section 03 30 00 – CAST-IN-PLACE CONCRETE.

Section 06 16 00 – SHEATHING.

Section 07 60 00 – FLASHING AND SHEET METAL.

Section 07 92 13 – ELASTOMERIC JOINT SEALANTS

Section 21 14 25 – ROOF DRAINS.

* + - 1. PERFORMANCE REQUIREMENTS
				1. Cold fluid applied polyurea hybrid roofing/waterproofing system is intended to perform as a continuous barrier against liquid water and to flash or discharge to the exterior incidental water. Membrane system is intended to be left exposed or receive an overburden of insulation and ballast or concrete pavers and shall accommodate movements of building materials as required with accessory sealant materials at locations such as: changes in substrate, perimeter conditions and penetrations.
				2. Installed roofing/waterproofing membrane system shall not permit the passage of water and will withstand the design pressures calculated in accordance with the most current revision of ASCE 7.
				3. Manufacturer shall provide all primary roofing/waterproofing materials that are physically and chemically compatible when installed in accordance with manufacturers current application requirements.
			2. SUBMITTALS
				1. Submittals: Comply with project requirements for submittals as specified in Division 01.
				2. Product Data: For each product.
				3. Shop Drawings: Manufacturer’s standard details and shop drawings for the specified system.
				4. Installer’s Authorization: Installer shall provide written documentation from the manufacturer of their authorization to install the system, and eligibility to obtain the warranty specified in this section.
				5. Manufacturer’ Certification: Certification showing full time quality control of production facilities and that each batch of material is tested to ensure conformance with the manufacturer's published physical properties.
				6. VOC Certification: Manufacturer’s certification that all roofing/waterproofing system products meet current Volatile Organic Compound (VOC) regulations as established by the State in which they are being installed; and stating total VOC content, in grams per liter, for all system components (i.e. primers, adhesives, coatings, etc.).
			3. QUALITY ASSURANCE
				1. Manufacturer’s Qualifications: Manufacturer shall demonstrate qualifications to supply materials of this section by certifying the following:

Membrane Manufacturer shall show evidence that the specified membrane has been manufactured by the same organization or direct affiliate for five years.

Membrane Manufacturer shall have available an in-house technical staff to assist the contractor when necessary in the application of the products and site review of the assembly.

* + - * 1. Installer’s Qualifications: The Contractor shall demonstrate qualifications to perform the Work of this Section by submitting certification or license by the roofing/waterproofing membrane manufacturer as a trained and authorized applicator of the product the installer intends to use.
				2. Source Limitations: All components listed in this section shall be provided by a single manufacturer or approved by the primary roofing/waterproofing manufacturer.
				3. Materials Compatibility: All materials included in the roofing/waterproofing assembly, as well as associated materials adhered to/applied beneath the roofing/waterproofing membrane shall have been tested and verified to be compatible.
				4. Final Inspection: Manufacturer’s representative shall provide to the Architect a comprehensive site visit report after the completion of the roofing/waterproofing system
				5. Applicable Regulations: Comply with local code and requirements of authorities having jurisdiction. Do not exceed VOC regulations as established by the State in which they are being installed, including total VOC content, in grams per liter, for all system components (i.e. primers, adhesives, coatings, and similar items).
				6. Roofing Terminology: Refer to ASTM D1079 and the glossary of the National Roofing Contractors Association (NRCA) Roofing and Waterproofing Manual for definitions of roofing terms related to this section.
			1. PRE-INSTALLATION CONFERENCE
				1. Prior to scheduled commencement of the roofing/waterproofing installation and associated work, conduct a meeting at the project site with the installer, architect/consultant, owner, manufacturer’s representative and any other persons directly involved with the performance of the Work. The Installer shall record conference discussions and to include decisions and agreements reached (or disagreements) and furnish copies of recorded discussions to each attending party. The main purpose of this meeting is to review foreseeable methods and procedures related to the Work.
			2. DELIVERY, STORAGE AND HANDLING
				1. Deliver all roofing/waterproofing materials to the site in original containers, with factory seals intact.
				2. Store all pail goods in their original undamaged containers in a clean, dry location within their specified temperature range.
				3. Do not expose materials to moisture in any form before, during, or after delivery to the site. Reject delivery of materials that show evidence of contact with moisture.
				4. Remove manufacturer supplied plastic covers from materials provided with such. Use “breathable” type covers such as canvas tarpaulins to allow venting and protection from weather and moisture. Cover and protect materials at the end of each workday. Do not remove any protective tarpaulins until immediately before the material will be installed.
				5. Materials shall be stored above 50°F (10°C) a minimum of 24 hours prior to application
			3. PROJECT CONDITIONS
				1. Weather: Proceed with roofing/waterproofing only when existing and forecasted weather conditions permit. Ambient/Substrate temperatures shall be above 35.6°F (2°C) when applying the roofing/waterproofing system.
				2. All surfaces to receive the roofing/waterproofing membrane shall be dry and free from water, dew, frost, snow and ice. Application of roofing/waterproofing membrane shall be conducted in well ventilated areas.
				3. Roofing/Waterproofing Membrane:

Roofing/waterproofing membrane is not intended to be exposed or in contact with a constant temperature below -22°F (-30°C) or in excess of 196°F (90°C). See technical data sheets for limitations, i.e., hot pipes and vents or direct steam venting.

Specified roofing/waterproofing membrane is non-flammable and VOC compliant. Consult container, packaging labels and Safety Data Sheets (SDS) for specific safety information.

Specified roofing/waterproofing membrane is resistant to gasoline, paraffin, fuel oil, mineral spirits, and moderate solutions of acids and alkalis, acid rain and detergents. Any exposure to foreign materials or chemical discharges shall be presented to membrane manufacturer for evaluation to determine any impact on the waterproof membrane assembly performance prior to warranty issuance.

* + - * 1. Contractor shall ensure adequate protection during installation of the roofing/waterproofing system.
			1. WARRANTY
				1. Warranty: Provide manufacturer’s standard Limited Labor & Materials warranty. Materials warranty shall be for a minimum of one year starting at the date of Substantial Completion. System warranty shall be for the following duration in accordance with specified system.

Warranty Length: 10 years.

Warranty Length: 20 years.

1. PRODUCTS
	* + 1. MANUFACTURER
				1. Basis-of-Design Manufacturer: Sika Corporation, 100 Dan Road, Canton, MA 02021. Toll Free 800-451-2504, www.us.sika.com. No substitutions without prior written approval by the Architect.
			2. ROOFING/Waterproofing SYSTEM
				1. Exposed System – Chemical Containment or Cooling Tower Areas with Sikalastic 702/701 SF.

Base Layer: Sikalastic 702, @80 mils wet film thickness; 20 sf/gal coverage rate approx.

Top Layer: Sikalastic 701 SF, @10-12 mils wet film thickness; 160 - 130 sf/gal coverage rate approx.

* + - * 1. Exposed Unreinforced System with Sikalastic 702/701 SF:

Base Layer: Sikalastic 702, @80 mils wet film thickness; 20 sf/gal coverage rate approx.

Top Layer: Sikalastic 701 SF, @10-12 mils wet film thickness; 160 - 130 sf/gal coverage rate approx.

* + - * 1. Unreinforced Protected Membrane System with Sikalastic 702:

Base Layer: Sikalastic 702, @40 mils wet film thickness; 40 sf/gal coverage rate approx.

Top Layer: Sikalastic 702, @40 mils wet film thickness; 40 sf/gal coverage rate approx.

* + - * 1. Reinforced System with Sikalastic 702 or 702/701 SF:

Base Layer: Sikalastic 702, @40 mils wet film thickness; 40 sf/gal coverage rate approx.

Reinforcement: PAREX Synergy Reinforcing Mesh 355

Top Layer: Sikalastic 702, @40 mils wet film thickness; 40 sf/gal coverage rate approx.

Top Layer, UV Protection: Sikalastic 701 SF, @10-12 mils WFT; 160 – 130 sf/gal coverage rate approx.

* + - 1. MEMBRANES AND COATINGS
				1. Base coat shall be Sikalastic 702 by Sika Corp, a two component, cold applied, self-smoothing, elastic polyurea based liquid roofing/waterproofing membrane.
				2. Base embedment coat with PAREX Synergy Reinforcing Mesh 355 reinforcement shall be Sikalastic 702 by Sika Corp, a two component, cold applied, self-smoothing, elastic polyurea based liquid roofing/waterproofing membrane.
				3. Sikalastic 702 THX by Sika Corp, a two component, elastic, thixotropic, hand applied, polyurea based liquid membrane for roofing/waterproofing detail work.
				4. Topcoat for UV protection shall be Sikalastic 701 SF by Sika Corp, a two component, 100% solids, low odor, high performance, polyaspartic top coat.
				5. Film Physical Property Requirements:

|  |  |  |
| --- | --- | --- |
| **Technical Data** | **Standard** | **Min requirement** |
| Description |  | An ETAG 005 accredited,elastic, UV-stable, liquid, cold applied, roof waterproofing system based on polyurea hybrid technology. |
| Tensile strength | EN ISO 527-3 | ~ 10.0 N/mm2  |
| Tensile strain at break | EN ISO 527-3 | Approx. 900% |
| Solar reflectance  | ASTM C1549 | Initial Solar Reflectance 0.874 |
| Thermal emittance  | ASTM C1371 | Initial Thermal Emittance 0.90 |
| Solar reflectance index  | ASTM C1549 | Initial SRI 110.6 |
| Overall thickness |  | ~ 2.3 mm (90 mils DFT) |
| System build-up |  | Primer: depending on substrate typeBase coat: Sikalastic®-702 @ 80 mils WFT, 80ft²/gallon (2.5 - 2.8 kg/m2)Top coat: Sikalastic®-701 SF @ 8-10 mils WFT, 200-160 ft²/gallon (0.3 kg/m2)Vertical surfaces: Sikalastic®-702 THX |
| **Classification categories according to ETAG 005** |  |
| External fire performance | EN 13501-5 | BRoof (t1) & BRoof (t4) |
| Reaction to fire | EN 13501-1 | Euroclass E |
| Working life |  | W2 (10 years) |
| Climatic zones |  | (M&S) Moderate & Severe |
| Resistance to imposed loads |  | Compressible substrates: P2Non-compressible substrates: P4 |
| Roof slope |  | S1 to S4 |
| Lowest surface temperature |  | TL4 (- 30°C) |
| Highest surface temperature |  | TH4 (+90°C) |
| Statement on dangerous substances |  | None contained |
| Water vapour resistance factor (µ) |  | 2962 |
| Water vapour diffusion |  | 4.98 m equivalent air layer thickness (Sd) |
| Resistance to wind loads |  | >50 kPa |

* + - 1. MEMBRANE REINFORCEMENT - FIBERGLASS
				1. Reinforcement for the roofing/waterproofing membrane system shall be PAREX Synergy Reinforcing Mesh 355 by Sika Corp, a 4.5 oz fiberglass, 38” wide X 150’ long roll, highly flexible and alkaline resistant for full or local reinforcement of Sikalastic 702 or 702 THX.
				2. Supplemental reinforcement of the Sikalastic roofing/waterproofing membrane system shall be Sika Joint Tape SA by Sika Corp., a self-adhering polymeric rubberized tape with woven polyester facer specifically designed for local reinforcement of the roofing/waterproofing membrane at structural cracks, expansion joints and transitions between dissimilar materials.
			2. FILLET BEAD AND PENETRATION SEALANT
				1. Sealant for fillet bead applications or gaps at penetrations shall be Sikaflex 11FC by Sika Corp., a one-part polyurethane sealant suitable for fillet bead transition compound to be applied prior to the installation of the membrane system at changes in substrate direction, sealing reglet terminations, cracks in the substrate and penetrations of the roof /waterproofing system.
				2. Exposed finish sealant shall be Sikaflex Hyflex 150 LM by Sika Corp., a one-part low modules hybrid sealant OR Sikasil WS-295. A one-part, low-modulus, weather sealing, silicone sealant suitable for finishing terminations at saw cuts and all UV exposed sealant terminations. SikaHyflex-150 LM is also suitable for fillet bead transition, changes in substrate direction, cracks in the substrate and penetrations of the roof before installation of the RoofPro membrane system
			3. PRIMERS
				1. Concrete and sealing cementitious substrates shall be primed with Sika Concrete Primer Lo-VOC by Sika Corp., a single component, rapid curing, high solids, moisture cured primer or Sikalastic Primer EP / Sikalastic Primer EP Rapid by Sika Corp., a two-component, cyclo-aliphatic, amine cured material.
				2. Green and damp concrete shall be primed with Sikalastic® GDC primer by Sika Corp., a 2-component, moisture mitigating epoxy primer for Green, Damp and Dry Concrete surfaces as well as plywood.
				3. Metal substrates shall be primed with Sikalastic® EP Primer/Sealer by Sika Corp., a two-component, cyclo-aliphatic, amine cured material with a high level of corrosion resistance for metal, bleed blocking on stable asphaltic surfaces, and chemically treated wood or the faster curing version Sikalastic® EP Primer Rapid by Sika Corp.
				4. Membrane over-coating primer shall be Sika Reactivation Primer by Sika Corp., a single component polyurethane-based primer specifically designed for the reactivation of roof /waterproofing system applications that exceed the open window prior to application of additional coats.
			4. CONCRETE REPAIR AND PATCHING
				1. Horizontal Cementitious repair mortar to repair bug holes, spalled areas, and other non-structural surface defects, or to slope decks shall be SikaQuick 1000 by Sika Corp., a two component, polymer-modified, Portland cement, fast-setting, trowel-grade mortar. Vertical & Overhead Cementitious repair mortar to repair bug holes, spalled areas and other non- structural surface defects shall be SikaQuick VOH.
				2. Epoxy resin to fill uneven areas and birdbaths shall be Sikadur-22 Lo-Mod.
			5. DRAINAGE MAT
				1. Soil, sand or stone ballast over burden:

Sika Drainage Mat 420: impermeable high flow dimpled polypropylene drainage core heat-bonded to a layer of non-woven polypropylene filter fabric on the exposed top side and a polyethylene membrane protection film on the substrate facing bottom side.

* + - * 1. Vegetated roof assemblies:

Sika Drainage Mat GRS: impermeable dimpled polystyrene drainage core that is perforated, then bonded to a root resistant non-woven polypropylene filter fabric on the exposed top side and non-woven polypropylene membrane protection fabric on the substrate facing bottom side. The core is installed dimpled side down to allow water retention within the cups. Excess water is collected and conveyed to a proper collection system, helping to control drainage flow.

* + - * 1. Freshly placed concrete or grout overburden:

Sika Drainage Mat 720: impermeable high flow dimpled polypropylene drainage core heat-bonded to a layer of woven polypropylene filter fabric on the exposed top side and a polyethylene membrane protection film on the substrate facing bottom side. Meant for overburden experiencing light traffic up to 18,000 psf.

Sika Drainage Mat 1000: high density polyethylene geonet drainage core with its ridges heat fused to a layer of non-woven polypropylene filter fabric on the exposed top side and a heavy duty non-woven polypropylene membrane protection fabric on the substrate facing bottom side. Meant for overburden experiencing heavy traffic up to 30,000 psf.

* + - 1. EXTRUDED POLYSTYRENE INSULATION
				1. Extruded polystyrene foam board insulation, either flat stock or tapered, meeting the requirements of ASTM 578 Type VI (40 psi – stone ballast or pavers in sand bed/direct application), Type VII (60 psi – concrete pavers on pedestals), or Type V (100 psi – superimposed loads). Insulation shall be Sika Sarnafil XPS.
			2. FILTER FABRIC
				1. Non-woven needle-punched polyester UV-stabilized mat, 3 oz./sq.yd., used between the extruded polystyrene insulation and stone ballast. Filter fabric shall be Sika 120 Fleece by Sika Corporation.
			3. CONCRETE PAVERS
				1. Architectural finish pavers meeting the following physical properties:

Compressive Strength, ASTM C140: Greater than 7,000 psi average min..

Flexural Strength, ASTM C293: Greater than 600 psi average min.

Water Absorption, ASTM C140: Not greater than 5%

Freeze/Thaw, ASTM C67: Less than 1% loss/dry weight (50 Cycles)

Centerload: Min. 1,750 lbs.

Weight: Min. 20 lbs/sq.ft. or as required for wind loading

* + - * 1. Pavers shall be manufactured by Hanover Architectural Products, Inc., Wausau Tile, Inc., or Westile, Inc. Paver pedestal systems shall be provided by the paver manufacturer.
			1. STONE BALLAST
				1. Standard graded stone ballast, either smooth river bottom stone or coarse aggregate, cleaned of fines and debris, meeting the gradation requirements of ASTM D448, as follows: #3, #4, or #24, to be applied at the minimum rate of 1,000 pounds per 100 square feet.
				2. Large graded stone ballast, either smooth river bottom stone or coarse aggregate, cleaned of fines and debris, meeting the gradation requirements of ASTM D448, as follows: #1 or #2, to be applied at the minimum rate of 1,300 pounds per 100 square feet.
1. EXECUTION
	* + 1. EXAMINATION
				1. Verify that surfaces and conditions are ready to accept the Work of this section. Notify Architect in writing of any discrepancies. Commencement of the Work in an area shall indicate Installer’s acceptance of the substrate.
				2. Surfaces shall be sound, dry, clean and free of oil, grease, dirt, excess mortar or other contaminants. Fill voids, gaps and spalled areas in substrate to provide an even plane. Strike masonry joints full flush.
			2. SURFACE PREPARATION
				1. Verify that the deck is clean and smooth, free of depressions, waves, or projections, and properly sloped to drains, valleys, eaves, scuppers or gutters. Verify that all roof openings or penetrations through the roof are secured back to solid blocking. Ensure all preparatory Work is complete prior to applying membrane.
				2. All surfaces shall be blown clean using best methods to remove any remaining loose debris.
				3. All cracks and voids greater than 0.040 inches shall be routed and caulked with a polyurethane sealant. Allow to cure per roof /waterproofing membrane manufacturer’s technical data sheets prior to over-coating with the specified roof /waterproofing membrane system.
				4. At all inside corners, gaps or voids at the juncture of the deck and penetrations apply a minimum 3/4 inch fillet bead of polyurethane sealant and allow to cure per roof /waterproofing membrane manufacturer’s technical data sheets prior to installing the roof /waterproofing membrane system.
				5. At all moving cracks, moving joints between dissimilar materials, and similar conditions, create a minimum 1 inch wide bond break utilizing bond breaker tape, centered over the crack or joint.
				6. Membrane terminations shall be established prior to project start-up and documented in shop drawings. Terminations shall occur in raked-out mortar joints, saw cut terminations or under installed counter-flashing materials.
				7. Use tape lines to achieve a straight edge detail. Remove tape while application is still wet for clean lines.
			3. SUBSTRATE PREPARATION
				1. Acceptable substrates include concrete, concrete block, solid wood/plywood sheathing and metal.
				2. Wood and Plywood Sheathing:

Solid wood sheathing shall be tongue & groove, or splined, or covered with a layer or plywood sheathing. Solid wood sheathing shall be not less than 3/4 inch (13 mm) thick.

Plywood sheathing shall be exterior grade, minimum 4 ply, and not less than 1/2 inch (12.7 mm) thick.

Preservatives or fire retardants used to treat the decking shall be compatible with roofing materials.

The deck shall be installed over joists that are spaced 24 inches (61 cm) o.c. or less and that all four sides bear on and are secured to joist and cross blocking. “H” clips are not acceptable.

Panels shall be installed with a 1/8 inch to 1/4 inch (3mm – 6mm) gap between panels and shall match vertically at joints to within (1/8 inch (3mm).

Decking shall be kept dry and roofed promptly after installation.

A ½” thick thermal barrier shall be installed and secured over all solid wood decks in accordance with wind uplift requirements.

Special attention is required for application over pressure treated wood: use Sikalastic EP Primer/Sealer as per Product Data Sheet. WOOD MOISTURE CONTENT SHALL NOT EXCEED 18% WOOD MOISTURE EQUIVALENT (WME) as measured by a Tramex moisture meter calibrated for WME.

* + - * 1. Structural Concrete:

Acceptable concrete substrates are limited to poured in place concrete decks.

Minimum deck thickness for structural concrete is 4 inches (10.2 cm).

Concrete surface to be ICRI CSP3-4 or equivalent.

Curing agents shall be checked for compatibility with specified roofing/waterproofing materials. Most curing agents shall be completely removed from the substrate by grinding, scarifying, or other mechanical means.

Concrete and masonry surfaces shall be low-pressure (5,000 psi or less) power-washed in accordance with ICRI Guideline No. 03732: Selecting and Specifying Concrete Surface Preparation for Sealers, Coatings, and Polymer Overlays to remove all dirt, debris or surface contamination that would compromise bonding of the specified roofing/waterproofing membrane system. Remove oil or grease with solvents, or detergent and water. Rinse surface clean of remaining cleaning agents.

Do not apply on substrates with moisture content greater than 4% by weight, measured by Tramex Concrete Moisture Encounter meter.

Application to Damp (moisture content greater than 4%) Concrete: Sikalastic® GDC Primer can be applied to damp concrete as soon as surface water has dissipated after rainfall or other sources of water have ceased.

Application to Green Concrete: Sikalastic® GDC Primer can be applied to horizontal concrete surfaces 48 hours after concrete pour (or when concrete is walkable) and vertical surfaces 24 hours after forms are removed.

Minimum substrate compressive strength > 3000 psi. at the time Sikalastic® GDC Primer is applied

* + - * 1. Metal Surfaces:

Exposed drain bowls, pipes, and other metal surfaces shall be cleaned by power tool cleaning (SSPC SP-3 or SP-11) to remove corrosion deposits back to a clean, bright metal followed by a solvent wipe prior to application of the specified primer.

* + - 1. PRIMING
				1. Concrete, Masonry and Wood:

Mix and apply specified primer for concrete/masonry/wood surfaces by brush or roller at the application rate shown on the technical data sheet. Porous, rough or absorbent surfaces will decrease coverage rates.

Allow to cure and dry in accordance with manufacturer’s technical data sheets.

* + - * 1. Metal:

Apply specified primer for metal surfaces to clean and prepared drain bowls and other metal surfaces by brush or roller at the application rate shown on the technical data sheet to achieve an overall wet film thickness of 6-8 mils. High porosity and roughness of the substrate will decrease coverage rates.

Allow to cure and dry in accordance with manufacturer’s technical data sheets.

* + - * 1. Existing Membrane Tie-In:

Apply specified reactivation primer to existing roof/waterproofing membrane, that is 48 hours past application, by roller at a maximum coverage rate of 250 sf/gallon. Allow to cure in accordance with manufacturer’s technical data sheets prior to application of subsequent roof/waterproofing membrane system.

* + - 1. MEMBRANE REINFORCEMENT
				1. Reinforcement of Cracks, Plywood, Joints, and Base/Curb Flashing Transitions:

For all locations where the specified membrane system is to be applied directly to the substrate surface, provide reinforcement of cracks and joints prior to applying the specified membrane system

For all moving cracks and joints, create a minimum 1-inch-wide bond break centered over the crack or joint by applying bond break tape centered over each crack or joint.

For all non-moving cracks and joints, rout and seal with Sikaflex polyurethane sealant.

For all horizontal-to-vertical transitions, provide a ¾” x ¾” Sikaflex polyurethane sealant cant.

Apply a minimum of a 3-inch-wide strip of Sika Joint Tape SA directly to the cured primer and roll with a hand roller to engage the adhesive.

Ensure reinforcement is not in tension during application.

* + - 1. COLD FLUID APPLIED MEMBRANE APPLICATION
				1. Install roofing/waterproofing membrane system in accordance with current technical data sheets and in accordance with Part 2 Section 2.2.
				2. Apply Sikalastic 702 THX base embedment coat to vertical wall and penetration surfaces by brush or with 1/2-inch nap roller to achieve a continuous and uniform minimum wet film thicknesses as specified in Part 2 section 2.2.
				3. Apply Sikalastic 702 to all prepped and primed horizontal surfaces with a notched squeeze or ½ inch nap roller to achieve a continuous and uniform minimum wet film thicknesses as specified in Part 2 section 2.2. Immediately the horizontal application with a spiked metal pin roller.
				4. Reinforced application with PAREX Synergy Reinforcing Mesh 355: Apply Sikalastic 702 to all prepped and primed horizontal surfaces with a notched squeegee or ½ inch nap roller to achieve a continuous and uniform minimum wet film thickness as specified in Part 2 section 2.2. Immediately the horizontal application with a spiked metal pin roller. Embed the Parex reinforcing scrim into the wet base coat and back roll or trowel to fully encapsulate the reinforcement.
				5. Overlap sheets of PAREX Synergy Reinforcing Mesh 355 a minimum of 3 inches at side laps and 6 inches at end laps.
				6. Extend membrane reinforcement vertically at adjacent wall surfaces in accordance with project details and specifications.
				7. Apply topcoat by nap roller or brush to achieve a continuous and uniform minimum wet film thickness as specified in Part 2 Section 2.2.
				8. Install all flashings in accordance with manufacturer’s construction details.
			2. PARAPET AND WALL FLASHINGS
				1. Clean, prepare and prime flashing substrate surfaces ready to receive membrane flashing applications.
				2. All parapet, wall, and curb flashings shall be provided with a cant bead of Sika 11FC sealant. Locally reinforce with Sika Joint Tape SA.
				3. Terminate roofing/waterproofing membrane system at raked-out mortar joints, termination saw cut joint, or under installed counter-flashing materials. Seal all mortar joints and saw cut joints with Sikaflex polyurethane sealant.
				4. Install metal counter flashings in accordance with details.
			3. drip edges and other metal flanged flashing
				1. Clean, prepare and prime metal flange surfaces ready to receive membrane flashing applications.
				2. Metal flanges are typically encapsulated between two membrane layers, usually by providing membrane flashing as a stripping ply over the metal flange, with the field or flashing membrane extending beneath the metal flange. It is also acceptable to install the stripping ply under the metal flange and extend the field or flashing membrane over the metal flange.
				3. For insulated roof assemblies, metal flanges shall be mechanically fastened through the first membrane layer to wood nailers. For direct to substrate membrane applications where the roof / waterproofing membrane is applied directly to the structural deck, metal flanges shall be mechanically fastened through the first membrane layer to the structural deck.
			4. ROOF DRAINS
				1. Clean, prepare and prime surfaces ready to receive membrane applications. Block drain bowl opening to avoid roofing/waterproofing material from entering the drainage system.
				2. Remove strainer baskets and clamping rings from the drain bowl assembly. Temporarily replace the bolts back into assembly to avoid miss-alignment of connections after membrane applications are completed.
				3. Extend the liquid roofing/ waterproofing material and membrane reinforcement directly into the bowl of the prepared drain.
				4. Remove drain blocks and allow the roofing/waterproofing system to fully cure dry prior to re-installing the drain bowl strainer assembly.
			5. ROOF PENETRATIONS
				1. Clean, prepare and prime surfaces ready to receive membrane flashing applications. Ensure that penetrations are secured to prevent movement.
				2. Install per standard details or job specific details for the project.
			6. AGGREGATE SURFACING
				1. Apply aggregate surfacing as specified for protective layer. DO NOT BROADCAST SAND INTO TOPCOAT
				2. Apply an additional 10-12 wet mil layer of Sikalastic 702 or 701 SF (depending on system) resin to cured roofing/waterproofing membrane as soon as membrane can be walked on without damage.
				3. Tile Overburden - Broadcast kiln-dried sand to refusal into the 10-12 wet mil layer of Sikalastic 702 wet resin layer and allow to cure. Remove all loose sand/aggregate.
				4. Non-Skid Finish - Broadcast kiln-dried sand to refusal into the wet resin layer and allow to cure. Remove all loose sand/aggregate. Apply an additional 10-12 wet mil layer of Sikalastic 701 SF resin to seal kiln-dried sand.
				5. Non-Skid Finish Broadcast & Backroll - Broadcast kiln-dried sand into the 10-12 wet mil layer of Sikalastic 701 SF and back roll to encapsulate the kiln dried sand. Allow to cure.
			7. APPLICATION OF PENETRATION SEALANT
				1. Seal reglet-based membrane terminations, heads of exposed mechanical fasteners, around penetrations, duct work, electrical and other apparatus extending through the roofing/waterproofing membrane with specified penetration sealant.
			8. FLOOD TEST (WHERE APPLICABLE/AS REQUIRED)
				1. Upon the completion of the roofing/waterproofing membrane system and associated terminations the contractor shall flood test the system. Provide temporary stops and plugs for the roof drains within the test area. Flood test with a minimum 2 inches of water for no less than 24 hours.
				2. Repair and retest the system for no less than 24 hours, report all deficiencies to the Architect. Remove temporary stops and plugs. No other Work is to proceed without prior direction from the Architect.
			9. MEMBRANE HIGH VOLTAGE ELD INTEGRITY TESTING (WHERE APPLICABLE/AS REQUIRED)
				1. Independent third-party testing companies are hired outside of Sika to perform high voltage ELD integrity testing of the completed Sikalastic RoofPro membrane.

B. Upon completion of the system installation and final inspection by manufacturer, the 3rd party testing company can then perform high voltage ELD integrity testing of the membrane.

C. Requirements for ELD testing, membrane has to cure a minimum of 14 days, membrane surface must be completely dry to perform testing, and high voltage testing method must be used: minimum 7.5 k/v.

D. Upon completion of ELD membrane testing a verbal report shall be provided to the A/E/C and manufacturer followed by a formal report. If ELD testing proves voids or inconsistencies in the membrane, all repairs are to be made by the installing applicator. Once satisfactory test results are received, all approved overburden should be installed within 48 hours.

* + - 1. ROOF PROTECTION
				1. Protect roofing/waterproofing Work from other trades until completion.
				2. Stage materials in such a manner that avoids foot traffic over completed roof areas.
				3. Provide temporary walkways and platforms to protect completed Work from traffic and point loading during the application process.
				4. Provide temporary membrane tie-ins and water-stops at the end of each workday and remove prior to commencement of Work the following day.
			2. PREFABRICATED COMPOSITE DRAINAGE AND PROTECTION MAT
				1. Install the drainage mat when it can be followed immediately by the installation of the extruded polystyrene insulation and pavers/ballast.
				2. Install the drainage mat on horizontal and vertical surfaces in accordance with the product data sheet. Lay out and position drainage mat, and allow to lay flat. Cut and closely fit drainage mat to perimeter and penetrations.
				3. Overlap filter fabric from adjacent sheets/rolls, and bond all fabric overlaps with Sikaflex sealant. Install supplemental filter fabric as required to ensure filter fabric continuity at flashing locations.
			3. INSTALLATION OF EXTRUDED POLYSTYRENE INSULATION
				1. Before the application of the insulation, any damage or deterioration to the composite drainage and protection mat shall be repaired.
				2. Loose lay insulation in a staggered manner, and tightly butt together all insulation boards. The maximum acceptable joint width is 3/8 inch. Cut and closely fit insulation within ¾ inches to perimeter and penetrations.
				3. For multi-layer insulation applications, the bottom layer shall be the thickest layer and shall be a minimum of 2 inches thick. Stagger the joints of each insulation layer.
				4. Vertical insulation applications can be spot adhered to the drainage mat and to additional insulation layers, utilizing an acceptable adhesive.
				5. Do not install damaged insulation boards.
			4. FILTER FABRIC
				1. Install filter fabric on horizontal and vertical surfaces over the extruded polystyrene insulation in accordance with the product data sheet.
				2. Lay out and position filter fabric. Cut and closely fit filter fabric to perimeter and penetrations, extending the filter fabric vertically to the height of the overburden.
				3. Overlap filter fabric to achieve 6 inch side and end laps. As required, bond all fabric overlaps with Sikaflex sealant to ensure filter fabric continuity prior to and during overburden installation.
			5. CONCRETE PAVERS
				1. Furnish and install concrete pavers in accordance with the product data sheet, including specified pedestal support system.
				2. Pavers shall be laid and fitted together to achieve a maximum joint width of 1/4 inch, and a maximum height variation between adjacent pavers of 1/4 inch.
				3. Plan paver installation to minimize use of paver segments smaller than one-half of a full paver.
				4. Cut pavers neatly to fit around penetrations and at perimeter, with a maximum gap of 1 inch.
				5. Do not install damaged paver units.
			6. STONE BALLAST
				1. Install stone ballast of the specified gradation at the prescribed application rate, in accordance with the most current revision of ANSI RP-4. Ensure full and even coverage.
			7. CLEAN-UP
				1. Work areas are to be kept clean, clear and free of debris at all times.
				2. Do not allow trash, waste, and/or debris to collect on the roof deck area. Trash, waste, and/or debris shall be removed from the roof on a daily basis.
				3. All tools and unused materials shall be collected at the end of each workday and stored properly off of the finished roof surface and protected from exposure to the elements.
				4. Dispose of or recycle all trash and excess material in a manner conforming to current EPA regulations and local laws.
				5. Properly clean the finished roof surface after completion, and make sure the drains and gutters are not clogged.
				6. Clean and restore all damaged surfaces to their original condition

END OF SECTION

The preceding specifications are provided by Sika Corporation as a guide for informational purposes only and are not intended to replace sound engineering practice and judgment and shall not be relied upon for that purpose. **Sika Corporation makes no warranty of any kind, either express or implied, as to the accuracy, completeness or the contents of these guide specifications**. Sika Corporation assumes no liability with respect to the provision or use of these guide specifications, nor shall any legal relationship be created by, or arise from, the provision of such specifications **SIKA SHALL NOT BE RESPONSIBLE UNDER ANY LEGAL THEORY TO ANY THIRD PARTY FOR ANY DIRECT OR CONSEQUENTIAL DAMAGES OF ANY KIND ARISING FROM THE USE OF THESE GUIDE SPECIFICATIONS.** The specifier, architect, engineer or design professional or contractor for a particular project bears the sole responsibility for the preparation and approval of the specifications and determining their suitability for a particular project or application.

Prior to each use of any Sika product, the user shall always read and follow the warnings and instructions on the product's most current Technical Data Sheet, product label and Material Safety Data Sheet which are available at www.sikausa.com or by calling (800) 933-7452. Nothing contained in any Sika materials relieves the user of the obligation to read and follow the warnings and instructions for each Sika product as set forth in the current Technical Data Sheet, product label and Material Safety Data Sheet prior to product use.