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SPECIFICATION 


Wabo®SurfaceMend 
Gray Polymer Concrete



PRODUCT INFORMATION

Manufacturer:	Watson Bowman Acme
		95 Pineview Drive
		Amherst, NY 14228
    
   (P) 800-677- 4WBA  
(F) 716-691-9239
www.wbacorp.com

Product Name:	Wabo®SurfaceMend

Product 
Description:  	Wabo®SurfaceMend is a two              component, moisture insensitive, 100% solid epoxy header material, with a specialty aggregate for use in exterior construction environments.

Intended 
Uses:              Expansion joint header for new
or restoration applications. Spall                                     repairs.  Patching airport                            concrete runways and tarmac
areas.






















A.	General

The work shall consist of furnishing, placing and bonding a gray two component, moisture insensitive, 100% solid epoxy header material, with a specialty aggregate in accordance with the details shown on the plans and the requirements of the specifications.  
Expansion Joint Manufacturer shall have a minimum ten (10) year’s experience specializing in the manufacture and supply of expansion joint headers	

B. Quality Control

Expansion Joint Manufacturer shall be  ISO-9001 shall provide written confirmation that a formal Quality Management System and Quality Processes have been adopted in the areas of, (but not limited to) Engineering, Manufacturing, Quality Control and Customer Service for all processes, products and their components.  

C.	Product

Provide a gray two component, moisture insensitive, 100% solid epoxy header and spall material as shown in the contract plans. 
Wabo®SurfaceMend is a unique high compressive strength mixture which monolithically bonds to steel or concrete.  The material absorbs traffic impact loads, evenly dispersing them into the deck while remaining flexible.

D.  Component and Materials

The Contractor shall furnish the selected manufacturer’s certificate of compliance that materials proposed will meet the requirements as set forth in these specifications: 

1. Liquid components shall meet the following requirements:

	PHYSICAL PROPERTY
	TEST METHOD
	REQUIRMENTS

	Liquid Components

	Color
	Visual
	Gray

	Tensile Strength
	D 638
	2,000 psi, min.

	Elongation at Break
	D 638
	60%, min.

	Hardness, Shore D
	D 2240
	45 – 75

	Gel Time
	AASHTO M 200-73
	15 minutes, min.

	Mixing Ratio
	
	1:1 by volume










2. Mixed unit shall meet the following requirements:
	PHYSICAL PROPERTY
	TEST METHOD
	REQUIRMENTS

	
	
	

	Mixed Unit

	Compressive Strength, 
	C 579, 
24 hr., Method B
	3,200 psi., min.

	Bond Strength
	C 882
	1,500 psi., min. 1

	Abrasion Resistance
	C 501, Taber H-22
	0.02, max.2

	1  Value listed either along bond line or at concrete break.

2  Value calculated using the following equation from ASTM C 501: 

           (Wo – Wf) / Wf

Wo = original weight of specimen and holder, g.
Wf = final weight of specimen and holder, g.



E.	Construction Requirements

Contractor shall submit product information and necessary details after the award of the contract.

Contractor shall ensure and properly prepare all substrates prior to installation in accordance with the Manufacturer’s installation guidelines. 

All materials shall be stored properly per Manufacturer’s recommendations.    

Contractor shall consult Manufacturer literature for working temperature range of deck prior to installation.  


F.	Payment
The accepted quantity of gray polymer concrete will be paid for at the contract unit price per cubic foot.    

Payment will be made under:

PAY ITEM			PAY UNIT
Gray Polymer Concrete	Cubic  Foot
Payment will be full compensation for all work necessary to complete the items including furnishing and installing the polymer concrete

[bookmark: _GoBack]LIMITED WARRANTY:
Watson Bowman Acme Corp. warrants that this product conforms to its current applicable specifications.  WATSON BOWMAN ACME CORP. MAKES NO OTHER WARRANTY, EXPRESS OR IMPLIED, INCLUDING ANY WARRANTY OF MERCHANTABILITY OR WARRANTY OF FITNESS FOR A PARTICULAR PURPOSE.  The sole and exclusive remedy of Purchaser for any claim concerning this product, including, but not limited to, claims alleging breach of warranty, negligence, strict liability or otherwise, is the replacement of product or refund of the purchase price, at the sole option of Watson Bowman Acme Corp.  Any claims concerning this product shall be submitted in writing within one year of the delivery date of this product to Purchaser and any claims not presented within that period are waived by Purchaser.  IN NO EVENT SHALL WATSON BOWMAN ACME CORP. BE LIABLE FOR ANY SPECIAL, INCIDENTAL, CONSEQUENTIAL (INCLUDES LOSS OF PROFITS) OR PUNITIVE DAMAGES.  Other warranties may be available when the product is installed by a factory trained installer.  Contact your local Watson Bowman Acme representative for details.  The data expressed herein is true and accurate to the best of our knowledge at the time published; it is, however, subject to change without notice.
Watson Bowman Acme Corp.  95 Pineview Drive, Amherst, NY 14228 
phone:716-691-7566 / fax: 716-691-9239 / web site: http://www.wbacorp.com                                          
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We create chemistry




