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Sika Corporation 

Industrial Flooring


201 Polito Avenue

Lyndhurst, NJ 07071

Phone 201.933.8800

Fax 201.933.6225
www.sikafloorusa.com
SECTION 09 96 59
Sika Descoglas® RM 
High Performance Fiberglass Matt Reinforced Wall & Ceiling Surfacing System with Aliphatic Urethane Topcoats
PART 1 - GENERAL

1.01
Related Documents

A.
Drawings and general provisions of the Contract, including General and Supplementary Conditions, apply to this section.

1.02
Summary

A.
This section specifies a fiberglass matt reinforced, decorative interior wall and ceiling coating system. 

B.
Sika Descoglas RM  High Performance Fiberglass Matt Reinforced Wall & Ceiling Surfacing System is a monolithic wall and ceiling coating system able to withstand severe impact and temperature fluctuations. System can be modified to meet specific project conditions upon consultation with Sika Technical Service.
1.03
References

A. 
ASTM D 522-88
Test Method for Mandrel Bend Test of Attached Organic Coatings

B. 
ASTM D 1044-90
Test Method for Resistance of Transparent Plastics to Surface Abrasion


C. 
ASTM D 1864-88
Test Method for Moisture in Mineral Aggregates

D. 
ASTM E 84-91
Test Method for Surface Burning Characteristics of Building Materials

E.  
ASTM D 5420-04
Test Method for Impact Resistance of Flat, Rigid Plastic Specimen by Means of a Striker Impacted by a Falling Weight (Gardner Impact)

1.04
System Performance Requirements

A.
Provide an epoxy wall and ceiling coating system that, when cured, produces the following typical properties:


PROPERTY
TEST METHOD
RESULT

Flexibility
ASTM D 522-88
Passes 1" mandrel




without cracking


Wear Resistance
ASTM D 1044-90
0.019 gm loss


Fire Resistance
ASTM E 84-91
Class A & B SystemsAvailable




Consult the manufacturer


Impact Resistance
Gardner Impact 
>160 in SYMBOL 183 \f "Symbol" \s 10 \h lb

1.05
Submittals

A.
Comply with Section 01 33 00 - Submittal Procedures.

B.  
Product Data:  Submit manufacturer's product data, including physical properties and colors available.

C.
Submit two mock-up sample coupons that are representative of the finished wall and ceiling surface, texture and color.


D. 
Maintenance Instructions:  Submit manufacturer's maintenance instructions, including maintenance procedures and materials, procedures for stain removal and surface repair, and recommended schedule for cleaning.

1.06
Quality Assurance

A.
Installer Qualification: Use only a manufacturer prequalified installer with documented project experience of a similar size and complexity.  

B.
Mock-up: On site, fabricate a panel approximately 100 sq. ft. (10 sq. m.) to demonstrate quality of finished wall and ceiling system, complying with manufacturer's instructions.Install panel where directed by architect/engineer. Maintain panel as a standard of quality for all installations.

1.07
Delivery, Storage and Handling

A.
Deliver product in factory packages, clearly marked with manufacturer's identification, printed instructions, lot numbers and shelf life expiration date for each component.

B.
Store materials at 50°F to 90°F (10°C to 32 °C) in dry environment away from sunlight, heat, or other hazards.

1.08
Project Conditions

A.
Maintain minimum substrate surface temperature of 60°F (12°C) for a minimum of 48 hours before, during and after installation, or until cured.

B.
Provide ventilation, lighting and clean, drinkable water supply.

C.
Advise other trades of fixtures and fittings not to be installed until system is cured, such as: radiators, painting, decorating, floor-supported equipment or cabinetwork, caulking, plumbing, fixtures, etc.

D.
Work areas shall be kept free of traffic and no trades shall be permitted in rooms during the application and curing of the coating.

E.
Protect adjacent surfaces from damage resulting from work of this trade.If necessary, mask and/or cover adjacent surfaces, fixtures, equipment, etc. by suitable means.

F.
Gypsum drywall is only suitable for dry areas.  Water-resistant board products are suitable in occasionally wet areas. Install drywall in accordance with board product manufacturer's directions and with the factory paper bound edge 1/4 inch (6.4 mm) above floor line.Tape and fill joints; fill all fastener heads and other indentations for smooth finished surface.

PART 2 - PRODUCTS

2.01
Manufacturer


A. 
Manufacturer shall be certified under ISO 9001:  All liquid materials, including primers, resins, curing agents, finish coats, and sealants are manufactured and tested under an ISO 9001 registered quality system.


B. 
Approved Manufacturer shall be Sika Corp., Industrial Flooring, 201 Polito Avenue, Lyndhurst, NJ 07071

Contact: Jim Hendley  ph  513-638-0519  email: Hendley.jim@us.sika.com
A. Fiberglass Matt Reinforced Resinous Wall and Ceiling System: Descoglas RM High Performance Fiberglass Matt Reinforced Wall and Ceiling Surfacing System.
1. Bughole Filler: Sikaquick Smooth or Sikadur Injection Gel as required. 
2. Primer: Sikafloor 2570 Waterbased Primer at 3-4 mils, coverage rate of 350-400 sq.ft./gal

3. Base Coat:  Sikagard 215 Wall Coating, 8-10 mils (coverage rate 160-200 sq.ft./gal) apply and lay 
               up fiberglass scrim. Fiberglass scrim shall be Hexcel Style 1528, 5.94 oz, 0.17 mm with a breaking strength of 250

 lbf/in.  Substitution of other scrims will not be considered as the type and weight of the fiberglass scrim greatly   affects system performance.
4. Saturant Coat:  Sikagard 215 Wall Coating, 6 – 7 mils coverage rate 240-260 sq.ft./gal

5. Level Coat(s):  Sikagard 215 Wall Coating, 6 – 7 mils coverage rate 240-260 sq.ft./gal/coat. Two coats may be     necessary in order to completely hide the fiberglass scrim.  
6. Topcoats:  Two coats of Sikagard 307W Single Component Urethane Wall Coating, 4-6 mils coverage rate 275-400 sq.ft./gal).
PART 3 - EXECUTION

3.01
Inspection

A.
Before starting work, ensure that environmental and site conditions are suitable for application and curing.

B.
Inspect surfaces for acceptability of levelness, moisture content and other critical factors at time of installation.

C.
Report in writing to architect/engineer, with copy to manufacturer, of deficiencies that could impair work.Surfaces must be approved by the certified contractor prior to application of the system.

3.02
Surface Preparation

A
Prepare surfaces in accordance with manufacturer's instructions.

B.
Surface must be clean, sound and dry prior to application.

C.
Pre-fill surface irregularities, holes and cracks in accordance with manufacturer's recommendations.

3.03
Mixing

A.
Comply with manufacturer's instructions for mixing procedures.

B.
Pre-mix each component before every batch to ensure uniformity.

C.
Carefully measure and mix the components together.

3.04
Installation

A.
Follow manufacturer's written instructions.

B.
Prime entire surface with recommended primer.

C.
Apply coating in accordance with manufacturer's instruction to a total thickness depending upon the agreed to requirements of the installation.

D.
Apply each coat at manufacturer's recommended coverage to provide uniform, dense surface.

E.
Allow proper cure time for each installation step.

F.
Allow the finished system to cure for a minimum of 7 days from completion before putting into service.
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END OF SECTION

See legal disclaimer and pertinent information following

All information provided by Sika Corporation (“Sika”) concerning Sika products, including but not limited to, any recommendations and advice relating to the application and use of Sika products, is given in good faith based on Sika’s current experience and knowledge of its products when properly stored, handled and applied under normal conditions in accordance with Sika’s instructions.  In practice, the differences in materials, substrates, storage and handling conditions, actual site conditions and other factors outside of Sika’s control are such that Sika assumes no liability for the provision of such information, advice, recommendations or instructions related to its products, nor shall any legal relationship be created by or arise from the provision of such information, advice, recommendations or instructions related to its products.  The user of the Sika product(s) must test the product(s) for suitability for the intended application and purpose before proceeding with the full application of the product(s).

Sika reserves the right to change the properties of its products without notice.  All sales of Sika product(s) are subject to its current terms and conditions of sale that are available at www.sikacorp.com or by calling 201-933-8800.  

Prior to each use of any Sika product, the user must always read and follow the warnings and instructions on the product’s most current Technical Data Sheet, product label and Material Safety Data Sheet that are available at www.sikaconstruction.com or 1-800-933-7452.  Nothing contained in any Sika materials relieves the user of the obligation to read and follow the warnings and instruction for each Sika product as set forth in the current Technical Data Sheet, product label and Material Safety Data Sheet prior to product use.

Quality Certification Numbers: Lyndhurst: FM 69711 (ISO 9000), FM 70421 (QS 9000), Marion: FM 69715, Kansas City: FM 69107, Santa Fe Springs: FM 69408

Descoglas® and Sikaguard® are registered trademarks of Sika Corporation, all rights reserved. 
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